Chemical Engineering Science 282 (2023) 119219

Contents lists available atScienceDirect

Chemical Engineering Science journal homepage: www.elsevier.com/locate/ces

| # Membrane process design for biohydrogen purification with simultaneous CO2 capture: Feasibility and techno-economic assessment Wenqi Xu a, Arne Lindbråthen a, Saravanan Janakiramb, Luca Ansalonib, Linfeng Lei c, * Liyuan Deng a, a Department of Chemical Engineering, Norwegian University of Science and Technology (NTNU), Trondheim NO-7491, Norway b Department of Sustainable Energy Technology, SINTEF Industry, 0373 Oslo, Norway c State Key Laboratory of Chemical Engineering, School of Chemical Engineering, East China University of Science and Technology, 130 Meilong Road, Shanghai 200237, China |  |  | check for updates |
| --- | --- | --- | --- |
| A R T I C L E I N F O |  | A B S T R A C T |  |
| Keywords: Membrane process Dark fermentative biohydrogen Hydrogen purification: CO2 capture Techno-economic assessment |  | In this work, a membrane separation process is designed and optimized to purify dark fermentative biohydrogen by removing CO2. A CO2-selective PVAm-based nanocomposite membrane was selected considering its high CO2/ H2 separation performance and unique features suitable for the process. We tested the membrane performances under the separation conditions to provide a more accurate simulation basis. Several design scenarios were investigated. A two-stage process with a recycle stream is determined as the optimal design, in which the specific cost for purifying H2 to 99.5 vol% with H2 loss of <10% reaches only 0.156 $/Nm3. The techno-economic feasibility study of biohydrogen purification with simultaneous CO2 capture was also performed through an alternative design by introducing a 3rd-stage using the same membrane or an H2-selective membrane. Adding a 3rd-stage membrane can capture and purify CO2 as a side product of various purities, which further decreases the H2 loss, leading to additional economic benefits. |  |

1.  Introduction

Carbon  emissions from  energy generation  and  the  consequentin-

crease of CO2  concentration in the atmosphere are believed to be the

direct culprit of climate change and environmental degradation, such as

global warming and rising sea level (Cartwright, 2021). As the primary

source of CO2 emission is using fossil fuels for energy generation (Nor-

ahim et al., 2018), the global energy structure can be shifted to non-

carbon-based fuels to reduce CO2  emissions. Hydrogen, as a clean en-

ergy carrier and energy vector, has been used invarious applications and

is considered a promising alternative to traditional fossil fuels. Today,

the most common hydrogen production is from natural gas-based inte-

grated gasification combined cycle  (IGCC) processes through energy-

intensive  separation  steps  at  elevated  operating  temperatures  and

pressures. Recently, although usually in a much smaller size than IGCC,

a renewable and sustainable process to produce biohydrogen through

biomass  conversion  by  dark  fermentation  has  attracted  increasing

attention (Nanda      al   2015;et., Younaset al., 2022). The conversion of

biomass provides high energy content biofuels. The dark fermentation

process operates under much lower temperatures and pressures and is

angi and Nanda, 2020; Younas et al., 2022).

easy to operate with low energy consumption (Nanda et al., 2015; Sar-

H2   production  streams  from  both  IGCC  and  dark  fermentation contain a large amount of CO2 and are saturated with water (Lee et al., 2011). Purifying H2  from the water-saturated CO2/H2  mixture is chal- lenging. Traditional H2purification technologies, such as pressure swing adsorption (PSA), cryogenic process, and absorption, are mostly energy intensive (Bernardo et al., 2020; Li et al., 2015) and have high specific cost for H2  purification, especially when a small-sized plant is consid- ered. Moreover, the presence of water reduces the separation efficiency of the above-mentioned H2 purification processes; thus, water should be removed as a necessary pre-treatment step before the separation when using these technologies.

Membrane technology was introduced for CO2 and H2 separation to purify  biohydrogen  from  dark  fermentation  in  this  work.  Although membrane separation is an emerging technology in hydrogen purifica- tion, it has shown enormous potential due to its small footprint, low operating and capital cost, few chemical additives, process flexibility,

*  Corresponding author.

E-mail address: liyuan.deng@ntnu.no (L. Deng).

https://doi.org/10.1016/j.ces.2023.119219

Received 9 July 2023; Received in revised form 20 August 2023; Accepted 23 August 2023 Available online 3 September 2023

0009-2509/© 2023 The Author(s). Published by Elsevier Ltd. This is an open access article under the CC BY license (http://creativecommons.org/licenses/by/4.0/).

化学工程科学 282 (2023) 119219

目录列表可在ScienceDirect上获取化学工程科学

期刊主页：www.elsevier.com/locate/ces

| 生物制氢与CO2同步捕集膜工艺设计：可行性与技术经济评估 徐文奇a 、阿恩·林德布拉滕a 、萨拉瓦南·贾纳基拉姆b 、卢卡·安萨洛尼b 、雷林峰c ，*邓丽媛a， |  | 奇ck foru日期. |
| --- | --- | --- |
| a 挪威科技大学化学工程系（NTNU），特隆赫姆NO-7491 ，挪威 b 挪威奥斯陆SINTEF 工业可持续能源技术部，邮编0373 c 中国华东理工大学化学工程学院化学工程国家重点实验室，中国上海市梅龙路130号，邮编200237 |  |  |
| A R T I C L E I N F O 关键词： 膜工艺 暗发酵生物氢氢纯化：CO2捕集技术经济评估 | A B S T R A C T |  |
|  | 本研究设计并优化了一种膜分离工艺，通过去除CO2来净化暗发酵生物氢。我们选择了一种基于PVAm的CO2选择性纳米复合膜，因其具有优异的CO2/H2分离性能及适用于该工艺的独特特性。为提供更精确的模拟依据，我们在分离条件下测试了膜性能，并研究了多种设计方案。最终确定采用两段式工艺并引入循环流作为最优设计，将H2纯化至99.5体积%且H2损失率<10%的单位成本仅为0. 156美元/标准立方米。同时通过引入第三阶段（采用相同膜或H2选择性膜）的替代设计，对生物氢纯化与同步CO2捕集的工艺经济可行性进行了研究。增加第三阶段膜可捕获并纯化不同纯度的CO2作为副产物，进一步降低H2损失率，从而带来额外经济效益。 |  |

## 1.   引言

能源生产过程中的碳排放及随之导致的大气CO2浓度上升，被认为是气候变化和环境退化（如全球变暖和海平面上升） 的直接元凶（Cartwr- ight ，2021） 。 由于CO2排放的主要来源是使用化石燃料发电（Nor- ahim等人，2018），全球能源结构可转向非碳基燃料以减少CO2排放。氢作为清洁能源载体和能量载体， 已被应用于多种场景，被视为传统化石燃料的有前景替代品。 目前最常见的氢气生产方式是通过天然气基的集成气化联合循环（IGCC）工艺，在高温高压下进行耗能分离步骤。近年来，尽管规模通常远小于 IGCC ，但通过暗发酵将生物质转化为生物氢的可再生可持续工艺正受到越来越多关注（Nanda 等人，2015； Yo- unas 等人，2022） 。生物质转化可提供高能量含量的生物燃料。暗发酵

该工艺在较低温度和压力下运行，且易于操作，能耗较低（Nanda等， 2015；Sar-angi和Nanda ，2020；Younas等，2022）。

来自IGCC 和暗发酵的H2生产流中含有大量CO2且被水饱和（Lee 等人，2011） 。从水饱和的CO2/H2混合物中提纯H2具有挑战性。传统H2提纯技术（如变压吸附PSA 、低温工艺和吸收法）大多能耗高（Berna- rdo 等人，2020； Li 等人，2015），且H2提纯的单位成本较高，尤其在考虑小型装置时。此外，水的存在会降低上述H2提纯工艺的分离效率；因此，在使用这些技术时，必须将水作为分离前的必要预处理步骤去除。

本研究采用膜技术对暗发酵产生的生物氢进行CO2和H2分离纯化。尽管膜分离是氢气纯化领域新兴技术，但其占地面积小、运行及资本成本低、化学添加剂少、工艺灵活性强等特点，展现出巨大应用潜力。

*  通讯作者

电子邮箱：liyuan.deng@ntnu.no（L. Deng）。

https://doi.org/10.1016/j.ces.2023.119219

2023年7月9日收到；2023年8月20日收到修订版；2023年8月23日接受

2023年9月3日在线发布

0009-2509/© 2023 作者（们）。由Elsevier Ltd. 出版。本文为CC BY许可下的开放获取文章（http://creativecommons.org/licenses/by/4.0/）。

W. Xu et al.

and high energy efficiency, especially forsmall to medium size plants (Czyperek et al., 2010; Han and Ho, 2020; Huang et al., 2022). Two different categories of membranes can be used for CO2/H2  separation, namely,  H2-selective  membranes  or  CO2-selective membranes.  H2-se- lective membranes allow H2  to transport through membranes and be purified at the                  side       lowpermeateat  pressures,such  as  in palladium membranes  (Atsonios  et  al.,  2014;  Sazali  et  al.,  2020),  polymeric membranes  (Han  and  Ho,  2021b;  Huang  et  al.,  2022),  and  carbon membranes  (Dai  et  al.,  2023;  Salleh  and  Ismail,  2015).  Franz  et  al. evaluated  the  H2  purification  process  for  an  IGCC  plant  by  process simulation  using   H2-selective  membranes  and   CO2-selective  mem- branes, respectively. They found that, due to the selectivity limitation, a single-stage  process  using  a  CO2-selective  membrane  cannot  reach  a separation efficiency of >85%. Toachieve the production specification, two or even three stages are needed (Franz and Scherer, 2010). Leiet al. reported a process using an H2-selective carbon membrane for CO2 and H2  separation from an IGCC plant  (Lei et al.,  2021). Later, He et al. studied  the  use  of the  same  H2-selective  carbon  membrane  on  bio- hydrogen from dark fermentation (He et al., 2021).

Since the molecular size of H2  (2.9 Å) is significantly smaller than

that of CO2  (3.3 Å) (Pal and Agarwal, 2021), so far, most developed

membranes for CO2/H2 separation are H2-selective; only a few CO2-se-

lective membranes have been reported in the literature. CO2-selective

membranes for H2  purification are usually based on materials of high

CO2  solubility  selectivity,  but  most  of them  still  exhibited  moderate

CO2/H2  separation  performances  since  H2  isnearly  the  smallest  gas

(Han and Ho, 2021b). Some ether oxygen-rich polymeric membranes

were  reported  for  excellent  CO2/H2  selectivity  but  require  very  low

separation temperature, i.e    − 20◦     (           al   2006), imp.,CLinet.,lying  that  a

very energy-intensive pre-cooling step is needed to reach the optimal

separation  conditions.  On  the  other  hand,  CO2-selective  membranes

following the facilitated transport mechanism have been reported with

exceptional  CO2/H2   separation  performance  by  Ho  and  co-workers,

especially  at elevated temperatures  (at  >100◦      (C)Yang  et  al.,  2020;

Zhao and Ho, 2012). Facilitated transport membranes contain CO2-af-

finitycarriers in the membrane matrix that reversibly react with CO2,

often in the presence of water (H¨agg and Deng, 2015; Rafiq et al., 2016;

Rivero et al., 2023). The hydration reactions enable a reverse selectivity

against the size difference, allowing CO2  transport through the mem-

brane while H2  stays and is enriched at the retentate side. The process

design and techno-economic feasibility of this type of membranes have

been studied for H2  purification from the IGCC process syngas (Chen

et al., 2021; Han and Ho, 2021a), but have not yet been considered for

biohydrogen purification of dark fermentation streams where the pro-

cess size is small and the separation is under moderate conditions (Lee

et al., 2011).

Inour previous study, a polyvinylamine  (PVAm)-based facilitated transport membrane incorporated with polyvinyl alcohol (PVA)-grafted- graphene  oxide  (GO)  (PVAm/(PVA-GO))  was  developed  (Xu  et  al., 2023). A CO2/H2selectivity of 22 and CO2permeability 61.6 Barrer (10 vol% CO2  in H2  with saturated water) under 1.7 bar at 25 ◦ C was re- ported.  The  performance  overcomes  the  CO2/H2   Upper-bound  (Lin et al., 2006) and is among the best-performing CO2-selective CO2/H2 separation membranes under similar testing conditions except for some reported works at elevated temperatures (Ansaloni et al., 2015; Tong and Ho, 2017; Yang et al., 2020; Zhao et al., 2014; Zhao and Ho, 2012), showing great potential for the purification of fermentative biohydrogen under mild separation conditions. It is worthy mentioning that the water vapour favors the facilitated transport membranes such as the mem- brane under discussion.

The  current  work  aims  to  design  and  optimize  a  highly  efficient process for biohydrogen purification using a CO2-selective membrane, i. e., PVAm/(PVA-GO) membrane, and to conduct the techno-economic feasibility  study  of the  designed  process.  Since  the  H2  streams  from both IGCC and dark fermentation are water-saturated, and the PVAm/ (PVA-GO) membrane works better in the water-swollen state, no pre-

Chemical Engineering Science 282 (2023) 119219

treatment is required to remove water vapor for CO2-selective mem- branes, which simplifies the process. Thus, the application of facilitated transport membranes is expected to be more advantageous. In addition, using the CO2-selective membrane process can keep the purified bio- hydrogen on the high-pressure side of the membrane, which is beneficial to the further utilization of the produced hydrogen. However, to the best of the  authors, knowledge, few  studies  on fermentative biohydrogen purification using CO2-selective membranes have been reported.

In  this  work,  membrane  separation  processes  were  designed  and evaluated by simulation studies. The performance data of the PVAm/ PVA-GO  membrane  under  the  given  conditions  were  systematically tested for a more accurate investigation of the process. The performance data were tested with a fully humidified CO2/H2  mixture with compo- sitions of 10 vol% CO2 in H2 and 40 vol% CO2 in H2 at temperatures of 25 ◦ C to 75 ◦ C, reflecting the expected 1st- and 2nd-stage feed conditions and the dark fermentation conditions, respectively. Membrane separa- tion processes were then designed and simulated with ChemBrane (a user-customized  membrane  module   solver)   integrated  with  Aspen HYSYS using the performance data at the given conditions. Both single- stage and two-stage membrane processes were investigated to check the process potentials. The process simulation targets at H2 purity of 99.5% as pure fuel with <10 % H2 loss, with which a low cost of biohydrogen production was achieved by using the 2-stage PVAm/(PVA-GO) mem- brane process with recycle. Based on the findings, a 3rd-stage membrane unit was also introduced to purify the enriched CO2  to achieve simul- taneous  CO2  capture;  sensitivity  analysis  of CO2  purity  as  the  target product purity was studied in this case. Cost estimation of the process was  performed,  including  operating  expenditure  (OPEX)  and  capital expenditure (CAPEX) related to the operating parameter of each mem- brane  stage,  which  was  further  related  to  the  membrane  areas  and power consumptions  (vacuum pump and compressor included). With the addition of a 3rd-stage membrane unit, the final products of the process include both high-purity H2with a much lower H2loss and high- purity CO2 as a side product, leading to a low specific cost for green H2 purification   with   simultaneous   CO2    capture   for   negative   carbon emission.

2.  Experimental

2.1.  Membrane preparation

The  PVAm/PVA-GO  nanocomposite  membranes  were  fabricated following the procedure detailed in (Xu et al., 2023). A brief description is given here for the readers, convenience. 3.0 wt% PVAm aqueous so- lution  was  purified  from  Lupamin®  9095  (BASF  AG,  Germany)  and diluted. Graphene oxide (GO, <100 mesh, from LayerOne, Norway) was dissolved  into  DI  water  with  sodium  hydroxide  (NaOH,  97  %,  from Sigma-Aldrich, Norway) to adjust the pH to  10 to prepare  1 mg/mL water suspension. GO solution was sonicated to ensure exfoliation and a thorough dispersion (Janakiram et al., 2020). Polyvinyl alcohol (PVA, Mw: 85,000–124,000, 87–89 % hydrolyzed, from Sigma-Aldrich, Nor- way) was dissolved into DI water and the according amount of dispersed GO solution was added into PVA solution with stirring under 60 ◦ C to yield PVA-GO solutions with the concentration of PVA and GO in the solution as 0.034 wt% and 0.046 wt%, respectively. Afterward, the CO2- selective  nanocomposite  flat-sheet  membranes  were  coated  on  com- mercial polysulfone ultrafiltration membranes as membrane substrates (GR40PP, 20 k MWCO, from Alfa Laval Nordic AS) using a dip coating machine  (KCV  NIMA,  Biolin  Scientific,  Finland).  The  coated  PVAm/ PVA-GO membranes were then dried under room condition (approx 6 h) and treated at 90 ◦ C for 1 h.

2.2.  Membrane performance testing

The prepared PVAm/(PVA-GO) membranes were tested using fully humid mixed gases of two compositions, i.e., 10 vol% CO2 in H2, and 40

W. 徐等                                                                                                               化学工程科学282 (2023) 119219

以及高能效 ， 尤其适用于中小型工厂（Czyperek 等人，2010；Han 和Ho，2020；Huang等人，2022） 。用于CO2/H2分离的膜可分为两类：H 2选择性膜和CO2选择性膜。H2选择性膜允许H2通过膜并在低压下于渗透侧进行纯化，例如钯膜（Atsonios等人，2014；Sazali等人，2020）、聚合物膜（Han 和Ho，2021b；Huang 等人 ，2022） 以及碳膜（Dai 等人 ，2023；Salleh 和Ismail，2015） 。Franz 等 人 通 过 工 艺 模 拟 评 估 了IGCC工厂中分别采用H2选择性膜和CO2选择性膜的H2纯化工艺。他们发现， 由于选择性限制，使用CO2选择性膜的单级工艺无法达到>85%的分离 效 率 。 要达 到 生产规格 ， 需要两 到三个 阶段（Franz 和 Scherer， 2010） 。Lei等人报道了一种使用H2选择性碳膜从 IGCC 工厂中分离CO2和H2的工艺（Lei 等人，2021） 。随后，He等人研究了同一H2选择性碳膜在暗发酵生物氢生产中的应用（He 等人，2021）。

由 于 H2  的 分 子 尺 寸 （2.9  A） 显 著 小 于 CO2（3.3  A）（Pal  和Agarwal ，2021），迄今为止，大多数用于CO2/H2分离的膜都是H2选择性膜；文献中仅报道了少数CO2选择性膜。用于H2纯化的CO2选择性膜通常基于高CO2溶解度选择性材料，但由于H2几乎是体积最小的气体（Han 和 Ho ，2021b）， 其中大多数仍表现出中等的CO2/H2 分离性能。一些富含醚氧的聚合物膜被报道具有优异的CO2/H2选择性，但需要极低的分离温度，即-20 ◦ C（Lin 等人，2006），这意味着需要非常耗能的预冷步骤才能达到最佳分离条件。另一方面，Ho及其同事报道了遵循促进传输机制的CO2选择性膜，其具有卓越的CO2/H2分离性能，尤其在高温条件下（>100 ◦ C）（Yang 等人，2020；Zhao 和 Ho ，2012） 。促进传输膜的膜基质中含有CO2亲和载体，这些载体可逆地与CO2反应，

通常在水存在下进行（H¨agg                              拉菲克等人，与邓，2015

年；        al 2016；Rivero等人，2023） 。水合反应实现了对尺寸差

异的逆向选择性，使得CO2能通过膜传输，而H2保留在截留侧并富集。此类膜的工艺设计与技术经济可行性已针对 IGCC 工艺合成气中H2的纯化进行了研究（Chen等人，2021； Han 和 Ho ，2021a），但尚未考虑用于暗发酵流体的生物氢纯化，其中工艺规模较小且分离条件适中（Lee等人，2011）。

在我们先前的研究中，开发了一种基于聚乙烯胺（PVAm）的促进传输膜 ，其与聚乙烯醇（PVA） 接枝氧化石墨烯（GO） 结合（PVAm/ (PVA-GO)）（Xu 等人 ，2023） 。该膜在25 ◦ C 、1.7巴压力下 ，对CO <sub>2</sub>/H<sub>2</sub>的选择性为22 ，CO<sub>2</sub>渗透率为61.6 Barrer（10 vol%CO<sub>2</sub>在H<sub>2</sub> 中，含饱和水） 。其性能超越了CO<sub>2/H<sub>2</sub>上限（Lin等人，2006），在类似测试条件下是表现最佳的CO<sub>2</sub>选择性CO<sub>2/H<sub>2</ sub>分离膜之一 ， 除部分报道的高温研究外（Ansaloni 等人，2015； Tong和 Ho ，2017； Yang 等人 ，2020； Zhao 等人 ，2014； Zhao 和Ho ，2012），显示出在温和分离条件下净化发酵生物氢的巨大潜力。值得一提的是，水蒸气有利于促进传输膜（如本研究讨论的膜）的性能。

本研究旨在设计并优化一种高效利用CO2选择性膜（即PVAm/(PVA- GO)膜）进行生物制氢的工艺流程，并对该工艺进行技术经济可行性研究 。 由于 IGCC 和暗发酵产生的H2气流均处于水饱和状态，且PVAm/ (PVA-GO)膜在水溶胀状态下性能更优，因此无需预处理。

对于CO2选择性膜而言，需要通过处理去除水蒸气以简化工艺流程。因此，应用促进传输膜预计更具优势。此外，采用CO2选择性膜工艺可使纯化后的生物氢保留在膜的高压侧，这对后续氢气的利用具有积极意义。然而据作者所知， 目前关于利用CO2选择性膜进行发酵生物氢纯化的研究报道仍较为有限。

在本研究中，通过模拟研究设计并评估了膜分离工艺。为更准确地探究工艺过程，系统测试了PVAm/PVA-GO膜在给定条件下的性能数据。测试采用完全湿润的CO2/H2混合气体，其组成分别为H2中10 vol%CO2和H2中40 vol%CO2 ，温度范围为25 ◦ C至75 ◦ C ，分别对应预期的一级和二级进料条件以及暗发酵条件。随后基于给定条件下的性能数据，使用集成于Aspen HYSYS 的ChemBrane（用户定制膜模块求解器）对膜分离工艺进行设计与模拟。通过研究单级和两级膜工艺以验证工艺潜力。该工艺模拟以99.5%纯度的H2作为纯燃料为目标，同时实现<10%的H2损失，通过采用带循环的两级PVAm/(PVA-GO)膜工艺，实现了低成本的生物氢生产。基于研究结果，我们还引入了第三级膜单元来净化富集的CO2 ，以实现同步CO2捕集；本案例中对以CO2纯度为目标产物纯度进行了灵敏度分析。对工艺进行了成本估算，包括与各膜级操作参数相关的运营支出（OPEX）和资本支出（CAPEX），这些参数进一步关联到膜面积和能耗（包括真空泵和压缩机） 。通过增加第三级膜单元，该工艺的最终产物包括损耗显著降低的高纯度H2以及作为副产物的高纯度CO2 ，从而实现了绿色H2净化与同步CO2捕集的低成本，为负碳排放提供了技术支撑。

## 2.   实验性

### 2.1.   膜制备

PVAm/PVA-GO纳米复合膜的制备方法详见（Xu 等人，2023）所述流程。为方便读者理解，此处简要说明如下：将3.0 wt%的PVAm水溶液从Lupamin® 9095（德国巴斯夫公司） 中纯化并稀释 。将氧化石墨烯（GO ，<100目，挪威LayerOne公司）溶解于去离子水中，并加入氢氧化钠（Janakiram 等人，2020）将pH调节至10 ，制得1 mg/mL的水悬浮液。对GO溶液进行超声处理以确保剥离和充分分散。将聚乙烯醇（PVA ，分子量：85,000-124,000 ，水解度87-89% ，挪威Sigma-Aldrich公司） 溶解于去离子水中，并在60 ◦ C下搅拌，将相应量的分散GO溶液加入PVA溶液中 ，得到PVA-GO溶液 ，其中PVA和GO的浓度分别为0.034 wt%和0.046 wt% 。随后，使用浸涂机（KCV NIMA ，BiolinScientific ，芬兰）将CO2选择性纳米复合扁平膜涂覆于商用聚砜超滤膜（GR40PP ，20k MWCO ，AlfaLavalNordicAS）上作为膜基材。涂覆后的PVAm/PVA-GO膜在室温条件下干燥（约6小时），并在90 ◦ C下处理1小时。

### 2.2.   膜性能检测

制备的PVAm/(PVA-GO)膜使用两种成分的完全湿润混合气体进行测试，即10体积% CO2在H2中， 以及40

vol% CO2  in H2 with feed pressure as 1.7 bar at varying temperatures,

from  25  ◦ C to  75  ◦ C. The permeation testing rig  is custom-made, as

described in (Dai et al., 2019). The sweep gas is nitrogen or argon at

approx. 1 bar with two different set-ups to verify the CO2/H2 separation

performance.  The  concentrations  of  CO2   and  H2   from  the  sweep/

permeate side were measured by a pre-calibrated gas chromatograph

(GC,  490  Micro  GC,  Agilent).  The  permeance  of CO2   ,  1 GPU =

0.001217  kPa•molhour•m2) can be obtained according to Eq. (1):

=                                                                            (1)

where Pi is the permeability of CO2 and Nperm is the total permeate flow rate that was measured using a bubble flow meter, yH2 O  is the mole fraction  of water  in  the  permeate  flow  calculated  according  to  the measured relative humidity and the vapor pressure (Φ = , which Φ

is relative humidity, pH2 O is the partial pressure of water vapor, and p*H2O

is the saturation vapor pressure of water at a given temperature) ac- cording to the testing condition, yi is the molar fraction of gas specie i in the permeate side, A is the effective membrane area, and pi,feed and pi,perm is the partial pressure of gas specie i in the feed and permeate side.

3.  Process simulation methods

3.1.  Process description

The   main   components   of  the   raw   product   stream   from   dark

fermentation are H2  and CO2,  with a small percent of CH4  (as an im-

purity here) and traces of other impurities, and saturated withwater

(Ghimire et al.,  2015). It should be notedthattheconcentrations of

impurities  can  be  tailored  by  applying  different  conditions  and/or

different  microorganisms  in  dark  fermentation  reactors  (Guo  et  al.,

2010). Thus, only components H2, CO2, and water are considered in this

work. Temperatures in the streams out of any dark fermentation tank

vary from 25 ◦ C to 80 ◦ C according to the species of microorganisms (Lee

et  al.,  2011).  The  conditions  of a  typical  dark  fermentation  product

stream are summarized in Table 1 (Lee et al., 2011). In order to produce

green H2 as high-quality fuel, the produced H2 purity was set to be 99.5

vol%, and the H2  loss was controlled to be below 10 vol% (He et al.,

2021; Lei et al., 2021).

The water-saturated gas stream from dark fermentation needs to be pressurized  for  separation.  Afterward,  the  pressurized  gas  is  cooled down to the given operating temperature (from 25 ◦ C to 75 ◦ C) and fed into  the  membrane  unit.  Single-stage  and  two-stage  CO2-selective facilitated transport membrane systems based on the PVAm/(PVA-GO) membrane are designed, as illustrated in Fig. 1.

As shown in Fig. 1 (a), the single-stage membrane system contains a compressor  (K-1) to increase the pressure from  1 bar to  1.7 bar  (the pressure of 1.7 bar was determined through experiment as mentioned before and applied throughout the study), a heat exchanger  (E-1) to decrease the stream temperature to the operating temperature after the compression, and a vacuum pump at the permeate side. Fig. 1 (b) pre- sents the two-stage process, where the 1st-stage and the 2nd-stage are designed to control the H2loss and H2purity, respectively, by the Adjust Unit  (ADJ),  in which  the membrane  area was used  as  an  adjustable variable and H2 loss and H2 purity were set as the target variables. The

Table 1

Dark fermentation biohydrogen product stream conditions.

| Parameters |  | Bio reactor conditions | Simulation basis |
| --- | --- | --- | --- |
| Temperature, ◦C |  | 25 ~ 80 | 25, 35, 45, 55, 65, 75 |
| Pressure, bar |  | 1 | 1 |
| Gas composition, vol.% | CO2 | 30–40 | 40 |
|  | H2 | 40–60 | 60 |
|  | CH4 | 0–5 | 0 |

two-stage membrane process consists of two CO2-selective membranes, two compressors (K-1 and K-2), two heat exchangers (E-1 and E-2), and two vacuum pumps at the permeate side of the respective membrane units. The gas stream from the fermenter combined with the recycle was fed into the compressor  (K-1) to reach the separation pressures. The enriched H2 from the 1st-stage membrane’s (M − 1) retentate side is then directly sent as the feed stream to the 2nd-stage membrane unit (M − 2) for the ultimate biohydrogen purification to produce purified H2. The permeate stream from the 2nd-stage membrane unit contains a large amount of hydrogen and is recycled back to the 1st-stage to avoid high H2  loss. Compressor (K-2) is applied in the recycle stream to compress the gas stream back to 1.0 bar to mix with the feed gas stream.

In  this  work,  only  membrane  configurations  in  the  asymmetric

cascade layout (the retentate flow from the 1st-stage feeding into the

2nd-stage), not the symmetric cascade (the permeate flow fed into the

2nd-stage), were considered for two reasons: (1) the membrane is CO2-

selective and based on facilitated transport; thus, feeding the permeate

stream (enriched with CO2) into the 2nd-stage will cause carrier satu-

ration in the facilitated transport membranes and consequently operate

below the optimal performance; and (2) if the 1st-stage permeate stream

(vacuum) is fed into the 2nd-stage, additional compression is needed,

adding extra capital cost and energy consumption.

3.2.  Simulation basis and general assumptions

Table 2 shows the simulation basis for the process based onthe outlet

flow conditions of dark fermentation (e.g., feed gas flow rate and tem-

perature) and experimental data (feed and permeate side pressures).

As  temperature  plays  a  critical  role  in  the  facilitated  transport mechanism, the selected membranes were experimentally evaluated at various temperatures in the expected range of the dark fermentation conditions to provide a more accurate simulation basis. The designed processes  were  simulated  by  Aspen  HYSYS  interfaced  with  a  user- customized module, ChemBrane (Deng and H¨agg, 2010). The simula- tion results based on ChemBrane show excellent consistency compared with  experimental  data,  as reported by  (Chu  et  al.,  2019). The  Pen- g–Robinson property package in Aspen HYSYS was used. Cross-flow, co- current  and  counter-current  flow  are  considered  in  the  ChemBrane. Cross-flow is typical for a spiral-wound module, while counter-current is typically used for hollow fibers.

The following assumptions were made to simplify the simulation:

- The membrane modules are assumed as hollow fiber modules with

the counter-currentflow.

- The compression ratio over each compressor stage is limited to 3.0

- A vacuum pump was used in the permeate side for all the membrane units, and it was simulated as an adiabatic compressor train.

- All compressors are modeled to have an adiabatic efficiency of 0.75.

-  Heat exchanger costs are not included in the study.

As an example of the simulation using ChemBrane interfaced with

Aspen HYSYS®, a flow sheet is shown in Fig. 2 for the designed 2nd-

stage process configuration. The 1st humidifier was set to simulate the

water saturated feed stream, and the 2nd humidifier was set to increase

the relative humidity to to optimal condition for CO2/H2 gas separation.

The cost of 2nd humidifier is not included in this work.

3.3.  Cost model

A rough economic evaluation was performed for the process design and optimization to minimize the capital and operating costs. As vac- uum pumps, compressors, and membrane units dominate the total cost in the membrane separation system, the capital costs were estimated only on these dominating equipment and membrane units. The capital cost  is  based  on  the  2021  Chemical  Engineering  Plant  Cost  Index (CEPCI), which gives a value of 708, and CAPCOST 2017, a software

vol%CO2在H2中的渗透率，进料压力为1.7巴，温度从25 ◦ C到75 ◦ C变化。渗透测试装置为定制设备，如（Dai 等人，2019）所述。扫气为约1巴的氮气或氩气，采用两种不同设置以验证CO2/H2分离性能。通过预校准的气相色谱仪（GC ，490 Micro GC ，Agilent）测量扫气/渗透侧的CO2

和H2浓度。 ，1 GPU=0.001217 kPa•molhour•m2) 可根据等式(1)

得到：

π =N积 (1 −  y H 2 O)y i                                                                                     (1)l A(pi，feed − pi，perm)

其中Pi为CO2的渗透率，Nperm为使用气泡流量计测得的总渗透流量，yH2 O 为根据测得的相对湿度和蒸气压计算的渗透流中水的摩尔分数 (Φ =  , 其中 Φ 相对湿度，pH2 O为水蒸气分压，p*H2O为给定温度下水的饱和蒸汽压）根据测试条件，yi为渗透侧气体组分i的摩尔分数，A为有效膜面积，and pi 、feedand pi 、perm分别为进料侧和渗透侧气体组分i的分压。

## 3.   过程模拟方法

3.1.   过程描述

暗发酵产物流的主要组分是H2和CO2 ，含有少量CH4（作为杂质）及其他微量杂质，并且水饱和（Ghimire 等，2015） 。需注意的是，通过在暗发酵反应器中应用不同条件和/或不同微生物，可调节杂质浓度（Guo等，2010） 。因此，本研究仅考虑H2 、CO2和水这三种组分。根据微生物种类，任何暗发酵罐流出流体的温度范围为25 ◦ C至80 ◦ C（Lee等， 2011） 。典型暗发酵产物流的条件总结于表1（Lee 等，2011） 。为生产绿色H2作为高质量燃料，将生成的H2纯度设定为99.5体积% ，并将H2损失控制在10体积%以下（He 等，2021； Lei 等，2021）。

来自暗发酵的水饱和气流需要加压进行分离。随后，将加压后的气体冷却至给定的操作温度（从25 ◦ C降至75 ◦ C），并送入膜单元。如图1所示，设计了基于PVAm/(PVA-GO)膜的单级和两级CO2选择性促进传输膜系统。

如图1(a)所示，单级膜系统包含压缩机(K-1)用于将压力从1巴提升至1.7巴（1.7巴的压力值通过实验确定，如前所述并贯穿整个研究），热交换器(E-1)用于将压缩后的流体温度降至操作温度， 以及位于渗透侧的真空泵。图1(b)展示了两级工艺流程，其中第一级和第二级分别通过调节单元(ADJ)控制氢气损失和氢气纯度，该单元以膜面积作为可调变量，将氢气损失和氢气纯度设定为目标变量。

表1

暗发酵生物氢产物流条件

| 参数 |  | 生物反应器条件 | 仿真基础 |
| --- | --- | --- | --- |
| 温度，◦ C |  | 25 ~ 80 | 25, 35, 45, 55, 65, 75 |
| 压力，bar |  | 1 | 1 |
| 气体组成，体积百分比 | 二氧化碳 | 30-40 | 40 |
|  | H2 | 40-60 | 60 |
|  | 甲烷 | 0-5 | 0 |

该两段式膜分离工艺包含两片二氧化碳选择性膜、两台压缩机（K-1和K-2）、两台换热器（E-1和E-2）， 以及位于各膜单元渗透侧的两台真空泵。发酵罐产生的气体与循环气体混合后，通过压缩机（K-1）输送至分离压力。第一级膜（M-1）截留侧富集的H2 随后直接作为进料流送入第二级膜单元（M-2），进行最终生物氢纯化以制备纯化H2 。第二级膜单元的渗透流富含氢气，为避免氢气大量流失，将其循环回第一级。压缩机（K-2）则用于压缩循环气体，将其压力降至1.0巴并与进料气体混合。

本研究仅考虑不对称级联布局（即第一级进料的截留液进入第二级）的膜结构配置，而非对称级联（即渗透液直接进入第二级） ，主要基于以下两点考量：(1)该膜具有CO2选择性且基于易化传输原理，若将富含CO2 的渗透液直接注入第二级，会导致易化传输膜的载体饱和，从而降低其最佳性能；(2)若将第一级的渗透液（处于真空状态）直接送入第二级，则需额外进行压缩处理，这不仅会增加设备投资成本，还会导致能耗上升。

### 3.2.   仿真基础和一般假设

表2展示了基于暗发酵出口流体条件（如进料气体流量与温度）及实验数据（进料侧与渗透侧压力）的工艺模拟依据。

由于温度在促进传输机制中起着关键作用，研究人员在暗发酵条件预期范围内的不同温度下对所选膜进行了实验评估， 以提供更精确的模拟基础。通过与用户自定义模块ChemBrane（Deng和Hägg，2010）对接的Aspen HYSYS 对设计流程进行模拟。根据（Chu 等人，2019） 的报道，基于ChemBrane的模拟结果与实验数据表现出极佳的一致性。本研究采用Aspen HYSYS 中的Peng-Robinson物性包 。ChemBrane中考虑了交叉流、 同向流和逆向流三种流动模式：交叉流常见于螺旋缠绕模块，而逆向流则多用于中空纤维。

为简化模拟，作出以下假设：

-  膜组件采用中空纤维结构，采用逆流方式。

-  各压缩机级的压缩比均不得超过3.0

-  所有膜单元的渗透侧均采用真空泵，该真空泵被模拟为绝热压缩机组。

-  所有压缩机均按绝热效率0.75进行建模。

-  本研究未包含热交换器成本。

作为使用ChemBrane与Aspen HYSYS ®接口的模拟示例，设计的第二阶段工艺配置流程图如图2所示。第一级加湿器用于模拟水饱和进料流，第二级加湿器用于将相对湿度提升至CO2/H2气体分离的最佳条件。本研究未包含第二级加湿器的成本。

### 3.3.   成本模型

为优化工艺设计以降低资本与运营成本，我们进行了初步经济评估。由于真空泵、压缩机和膜分离单元在系统总成本中占比最高，因此仅对这些核心设备及膜分离单元的资本成本进行估算。资本成本依据2021年《化工厂成本指数》 （CEPCI ）确定，该指数数值为708 ， 同时参考了2017年Capcost软件数据。

Fig. 1. Process flow diagram of a) a single-stage and b) a two-stage membrane system for biohydrogen purification.

Table 2

Simulation parameters for the biohydrogen purification process.

| Feed gas flow rate (dry base), m3(STP)/h | 3000 |
| --- | --- |
| Temperature, ◦C | 25 ~ 75 |
| Feed pressure, bar | 1.7 |
| Permeate pressure, mbar | 400 |

basedon  (                    al    2Turtonet.,008),  was  used  for  capital  cost  estimation.

Carbon steel rotary compressors (18 kW ~ 900 kW) were used for this

application. It is worth mentioning that under relatively low tempera-

tures with high H2purity, hydrogen embrittlement should be considered

when selecting materials for equipment and pipes. But, in this work, the

cost calculation.

hydrogen embrittlement issue was not considered to simplify the capital

The purchase cost, C0p , of rotary compressors is estimated by Eq. (2), log10 C0p = K1 + K2 log10 (Q) + K3 [log10 (Q)]2                                                                         (2)

where Q is the power consumption of compressors, and K1, K2, and K3

are constants of rotary compressors for cost estimation as 5.0355(K1),

− 1.8002(K2), and 0.8525(K3), respectively  (Turton et al., 2008). The

bare module cost,  CBM,  is  calculatedfor compressors  cost estimation

based on the purchase cost of rotary compressors and a bare module

factor, FBM, as shown in Eq. (3) (Turton et al., 2008).

CBM  = C0pFBM                                                                                                                                             (3)

The total module cost,CTM, isestimated by the bare module cost, and the grassroots cost, CGR, can be further evaluated by the total module cost, as illustrated in Eqs. (4) and (5).

where n is the number of equipment and C0BM,i is the bare module cost in

Fig. 2. Flow sheet of the 2nd-stage membrane process in Aspen HYSYS® .

图1.生物制氢纯化系统流程示意图：a) 单级膜系统；b) 双级膜系统。

表2

生物氢净化工艺的模拟参数。

| 原料气流量（干基），m 3（标准状态）/h | 3000 |
| --- | --- |
| 温度，◦ C | 25 ~ 75 |
| 进料压力，bar | 1.7 |
| 渗透压，毫巴 | 400 |

基于Turton 等人（2008年）的研究成果，本研究采用该方法进行资本成本估算。具体应用中选用碳钢材质的回转压缩机（功率范围18千瓦至900千瓦） 。需要特别说明的是，在低温环境下且氢气纯度较高时，设备与管道选材需考虑氢脆风险。但为简化资本成本计算流程，本研究未纳入氢脆因素考量。

旋转压缩机的购买成本C0p通过等式(2)估算，log10 C0p=K1 + K2 log10

(Q) +K3 [log10(Q)]2              (2)

其中Q表示压缩机的功耗，K1 、K2和K3分别为用于成本估算的回转压缩机常数，分别为5.0355（K1）、-1.8002（K2）和0.8525（K3）（Turton等，2008） 。裸模块成本CBM是基于回转压缩机的采购成本和裸模块系数FBM计算得出的，如等式(3)所示（Turton 等，2008）。

CBM  = C0pFBM                                                                                                                                             (3)

总模块成本CTM 由裸模块成本估算得出，基层成本CGR可通过总模块成本进一步评估，如公式(4)和(5)所示。

∑n

其中n为设备数量，C0BM 、i为裸模块成本

图2.Aspen HYSYS ®第二阶段膜工艺流程图。

the base condition. For the membrane unit, 50 $/m2  is the estimated price  of  PVAm/(PVA-GO)  membranes,  including  material  costs  for membranes  and  modules  and  the  installation  cost.  Annual  capital- related cost (CRC) for the whole system can be evaluated to be 20% of the CGR and 28% of the membrane module cost, CM. To simplify the cost estimation, only electricity and labor cost are considered as operating expenditures  (OPEX),  where  the  electricity  cost  is  0.05  $/kWh,  and labor cost is 17 $/h, which is the average standard all over the world (He et al., 2021; Lei et al., 2021) with the total operating hour of 7500 h/ year. The specific cost of H2  purification ($/Nm3  H2  produced) can be calculated by Eq. (6).

In this work, the lifetimes of the membrane, equipment, and project are assumed as 5 years, 20 years, and 20 years, respectively.

4.  Results and discussion

4.1.  Gas separation performance

The membrane performances of the CO2-selective PVAm/(PVA-GO)

membranes are given in Table 3, including two feed compositions (CO2/

H2  mixtures of 40% CO2  and 10% CO2) at varying temperatures. The

experimental data are given inthe Supporting Information (Fig. S1). The

H2-selective carbon molecular  sieving membrane performances  (50%

CO2) at varied temperatures are listed in Table 4. The CO2  and H2 per-

meances presented in Tables 3 and 4 at the given temperature are based

on the linear fitting data from the experimental results.

For CO2-selective membranes (see Table 3), when the feed gas con- taining 40 vol% CO2in H2, CO2permeance decreases, and H2permeance increases  with  increasing  temperature.  This  trend  shows  that,  under relatively high CO2  concentrations, the effect of CO2  sorption on gas permeation  is  more  significant  than  diffusion,  which  decreases  with increasing temperature. However, when the feed        containgass only 10 vol% CO2  in H2  (Table.3), both CO2  permeance and H2  permeance in- crease with increasing temperature, implying that the effect of diffusion becomes more significant in the gas transport through the membrane.

It needs to be noted that due to the measurement limitation in the concentration of water at the permeate side, the water permeance of the membranes  could  not  be  determined  by  the  current  experiments. Therefore, it is assumed that the water permeance in a membrane is the same as the permeance of the favorable gas through the membrane, a method adapted from the literature (He et al., 2021; Lei et al., 2021), i. e., the water permeance is assumed the same as the H2permeance in H2- selective  membranes  and  as  the  CO2   permeance  in  CO2-selective membranes.

All the  gas  separation performance results from the  experimental study were obtained with a standard deviation lower than 10%. Thus, the deviations are not presented in the Tables.

Table 3

Membrane performances of the CO2-selective PVAm/(PVA-GO) membrane.

| Temperature (◦C) | 40 vol% CO2 in H2 |  | 10 vol% CO2 in H2 |  |
| --- | --- | --- | --- | --- |
|  | CO2 permeance (GPU) | H2 permeance (GPU) | CO2 permeance (GPU) | H2 permeance (GPU) |
| 25 | 58.6 | 3.2 | 14.3 | 0.8 |
| 35 | 53.4 | 3.8 | 21.4 | 1.5 |
| 45 | 48.9 | 4.6 | 31.1 | 2.6 |
| 55 | 45 | 5.4 | 44.4 | 4.4 |
| 65 | 41.6 | 6.3 | 62 | 7.3 |
| 75 | 38.7 | 7.3 | 84.8 | 11.7 |

Table 4

Membrane performances of H2-selective carbon molecular sieving membranes, tested with 50 vol% H2  in CO2  (He et al., 2021).

| Temperature (◦C) | H2 permeance (GPU) | CO2 permeance (GPU) |
| --- | --- | --- |
| 25 | 27.3 | 0.8 |
| 35 | 34 | 1.1 |
| 45 | 41.9 | 1.3 |
| 55 | 50.8 | 1.5 |
| 65 | 61 | 1.8 |
| 75 | 72.4 | 2.1 |

4.2.  Process optimization

4.2.1.  Single-stage membrane process

In the single-stage membrane process, the raw biohydrogen stream from dark fermentation is fed directly to the PVAm/(PVA-GO) mem- brane unit after being compressed to 1.7 bar. As the performance of the selected  facilitated  transport  membrane  varies  significantly  with  the temperature, the influence of feed temperature, which is controlled by fermentative  temperature  from  25  ◦ C  to  75  ◦ C,  was  investigated  by simulation. The required membrane area was adjusted to achieve an H2 loss  of  <  10  %. The  obtained  H2  purities  at  given  temperatures  are presented in Fig. 3. With increasing operating temperature in the single stage, the achieved H2  purity decreases. This is expected as the mem- brane exhibits higher CO2 permeance but decreasing CO2/H2 selectivity with  increasing  temperature  for  the  CO2/H2   mixture  of  40%  CO2. Therefore,  the  optimal  temperature  for  a  single-stage  membrane  is determined to be at 25 ◦ C when targeting high purity, where the highest H2 purity of 87 vol% is obtained.

The operating temperature of 25 ◦ C was used in further studies of the dependence of H2  purity on the H2  loss. Fig. 4 shows the relationship between H2 loss and H2 purity in a single-stage membrane system (the blown dataset) and the membrane area required to control the given H2 loss (the blue dataset). As shown in the figure, the H2 purity (retentate side) decreases with a lower H2  loss (controlled at the permeate side), and the required membrane area at a given H2loss shows a similar trend as expected. In the case of achieving a lower H2 loss, less H2 transports through a smaller membrane area; hence the retentate H2  purity de- creases. For a higher H2  purity, more CO2  must permeate through the membrane, which requires a higher membrane area, thus leading to a higher H2 loss. Therefore, there is a clear trade-off between H2 loss and

Fig. 3. Effect of single-stage feed temperature on the H2  purity with fixed H2 loss as 10 %.

基础条件。对于膜组件，PVAm/(PVA-GO)膜的预估价格为50美元/平方米，包括膜和组件的材料成本以及安装成本。整个系统的年度资本相关成本（CRC）可评估为CGR的20%和膜组件成本CM 的28% 。为简化成本估算，仅将电力和人工成本视为运营支出（OPEX），其中电力成本为0.05美元/千瓦时，人工成本为17美元/小时，这是全球平均标准（He等， 2021； Lei 等，2021），总运营时间为每年7500小时。H2纯化的具体成本（$/Nm3 H2产量）可通过等式(6)计算。

本研究中，膜组件、设备及项目的预期使用寿命分别设定为5年、20年和20年。

## 4.   结果与讨论

### 4.1.   气体分离性能

CO2选择性PVAm/(PVA-GO)膜的膜性能见表3 ，包括两种进料组成（40%CO2与10%CO2的混合气体）在不同温度下的数据。实验数据见支持信息（图S1） 。H2选择性碳分子筛膜性能（50%CO2）在不同温度下的数据列于表4 。表3和表4中给出的CO2与H2在特定温度下的渗透率数据，均基于实验结果的线性拟合数据。

对于CO2选择性膜（参见表3）， 当进料气体中含40 vol% CO2的H2时，CO2渗透率随温度升高而降低，H2渗透率随温度升高而增加。这一趋势表明，在相对较高的CO2浓度下，CO2吸附对气体渗透的影响比扩散更为显著，而扩散效应随温度升高而减弱。然而，当进料气体中仅含10 vol%CO2的H2时（ 表3），CO2渗透率和H2渗透率均随温度升高而增加，这意味着在气体通过膜的传输过程中，扩散效应变得更加显著。

需要指出的是， 由于渗透侧水浓度的测量限制，当前实验无法测定膜的水渗透率。因此，我们假设膜中的水渗透率与有利气体通过膜的渗透率相同，该方法改编自文献（He 等人，2021； Lei 等人，2021），即假设水渗透率与H2选择性膜中的H2渗透率以及CO2选择性膜中的CO2渗透率相同。

实验研究中所有气体分离性能结果的标准偏差均低于10% 。因此，表中未列出偏差数据。

表3

CO2选择性PVAm/(PVA-GO)膜的膜性能。

| 温 度 ( ◦ C） | 40体积百分比CO2在H2 中 |  | 10体积百分比CO2在H2 中 |  |
| --- | --- | --- | --- | --- |
|  | 二氧化碳磁导率 | H2 磁导率 | 二 氧 化碳 磁导率 | H2 磁导率 |
| 25 | 58.6 | 3.2 | 14.3 | 0.8 |
| 35 | 53.4 | 3.8 | 21.4 | 1.5 |
| 45 | 48.9 | 4.6 | 31.1 | 2.6 |
| 55 | 45 | 5.4 | 44.4 | 4.4 |
| 65 | 41.6 | 6.3 | 62 | 7.3 |
| 75 | 38.7 | 7.3 | 84.8 | 11.7 |

表4

H2选择性碳分子筛膜的膜性能，使用50 vol%H2在CO2 中进行测试（He 等人， 2021）。

| 温度 (◦ C） | H2通透性（GPU） | CO2通量 (GPU) |
| --- | --- | --- |
| 25 | 27.3 | 0.8 |
| 35 | 34 | 1.1 |
| 45 | 41.9 | 1.3 |
| 55 | 50.8 | 1.5 |
| 65 | 61 | 1.8 |
| 75 | 72.4 | 2.1 |

### 4.2.   工艺优化

#### 4.2.1.   单级膜工艺

在单级膜工艺中，来自暗发酵的原始生物氢流经压缩至1.7巴后直接送入PVAm/(PVA-GO)膜单元。 由于所选促进传输膜的性能随温度变化显著，通过模拟研究了由25 ◦ C至75 ◦ C发酵温度控制的进料温度的影响。通过调整所需膜面积以实现H2损失<10% 。给定温度下获得的H2纯度如图3所示。随着单级操作温度升高，获得的H2纯度降低。这符合预期，因为对于40%CO2的CO2/H2混合物，膜表现出更高的CO2渗透率，但CO2/ H2选择性随温度升高而降低。因此，当追求高纯度时，单级膜的最佳温度确定为25 ◦ C ，此时获得最高H2纯度87 vol%。

在进一步研究H2纯度与H2损失的关系时，采用了25 ◦ C的操作温度。图4展示了单级膜系统中H2损失与H2纯度的关系（吹扫数据集） 以及控制给定H2损失所需的膜面积（蓝色数据集） 。如图所示，H2纯度（截留侧）随H2损失（渗透侧控制） 的降低而下降，且给定H2损失时所需膜面积呈现出与预期相似的趋势。当实现较低H2损失时，通过较小膜面积的H2传输量减少，因此截留侧H2纯度降低。对于较高的H2纯度，必须有更多CO2通过膜渗透，这需要更大的膜面积，从而导致更高的H2损失。因此，H2损失与

图3.单级进料温度对H2纯度的影响（固定H2损失为10%）。

Fig. 4. Effects of H2  loss on membrane area (blue line) and the trade-off be- tween H2 purity and H2 loss (brown line) in the single-stage membrane process, at 25 ◦ C, 1.7 bar.

H2  purity in a single-stage membrane system, and one more stage is needed for biohydrogen purification to achieve the required high purity of H2  (99.5 vol%) and low H2 loss (<10%).

4.2.2.  Two-stage membrane process

Since the operating temperature significantly influences gas sepa- ration performances ofthe PVAm/(PVA-GO) membrane, it will certainly further affect the capital cost and specific cost of the H2  purification process. Thus, the operating temperatures of each membrane unit are optimized  through  process  simulation  and  techno-economic  analysis with fixed H2  loss and H2  purity. According to the experimental data with the feed gas of 40 vol% CO2 in H2, a higher operating temperature results in a lower CO2  permeance and simultaneous loss in selectivity. Since membranes of a lower CO2  permeance lead to an increase in the required  membrane  area  for  the  separation  to  meet  the  H2   purity requirement, an additional membrane area is required to compensate for the permeance loss. Consequently, the CRC, determined by the mem- brane module cost, becomes a function of the operating temperature. Hence, theoperating temperature of the membrane units can be opti- mized to minimize the capital cost and specific cost of H2 purification.

The effect of operating temperature on membrane area, power con- sumption, and costs is studied in the designed two-stage, CO2-selective membrane process (Marked as scenario A) in this work. The total H2loss of 10% and H2  purity of 99.5 vol% (dry base) are fixed as the targets; only the temperatures in the 2nd-stage are allowed to vary. Table 5 lists the details of scenario A for the optimizations of operating temperatures of membrane units in the two-staged membrane system, where in case A1, the 2nd-stage temperature is fixed to be 25 ◦ C while the 1st-stage membrane is allowed to vary to optimize the 1st-stage temperature. In the case of A2, the optimized 1st-stage temperature based on case A1 will be fixed to study the effect of temperature change in the 2nd-stage membrane module.

When the feed stream temperature of the  1st-stage membrane in- creases from 25 ◦ C to 75 ◦ C, the process can be easily implemented since

Table 5

Scenario A for optimizations of operating temperatures in membrane units.

| Scenario | T, ◦C 1st-stage | T, ◦ C 2nd- stage | Pfeed, bar | H2 purity, % (dry base) | H2 loss, % |
| --- | --- | --- | --- | --- | --- |
| A1 A2 | 25 ~ 75 Optimized | 25 25 ~ 75 | 1.7 | 99.5 | 10 |

the fermentative temperature of dark fermentation is from 25 ◦ C to 75 ◦ C (Lee et al., 2011).

When the 1st-stage operating temperature increases, the membrane

area of the 1st-stage slightly changes, first decreasing then increasing at

55 ◦ C, while that of the 2nd-stage increases notably and almost linearly.

Since the CO2  permeance of the membrane increases and CO2/H2  se-

lective decreases with increasing temperature, the operating tempera-

ture shows a significant influence on the membrane area in the 1st-stage

membrane unit. However, the 1st-stage membrane area is also affected

by the recycle stream; increasingthe operating temperature of the 1st-

stage membrane unit increases the needed ratio for the recycle stream

and thus increases the membrane area. The sum of the two effects makes

a slightly curved downtrend of the 1st-stage membrane area with tem-

perature, but the overall power consumption increases monotonously

due  to  the  much  larger  amount  of  the  recycle  stream  to  meet  the

requirement of H2 purity and H2 loss, as presented in Fig. 5 (a) and (b).

As the membrane unit cost dominates the CRC, the CRC value reaches

trend, as shown in Fig. 5 (c). Thus,the optimal operating temperature of

the minimum, and the specific cost of H2  production follows the same

the  1st-stage feed stream is set to be  25  ◦ C,  and the  specific cost of

purifying H2 at this temperature is 0.266 $/Nm3.

After the optimal feed stream temperature of the 1st-stage is deter- mined to be 25 ◦ C, the effect of operating temperature at the 2nd-stage was investigated by process simulation with the 1st-stage temperature fixed as 25 ◦ C and the 2nd-stage temperature varying from 25 ~ 75 ◦ C, as the scenario A2. It should be pointed out that the feed gas mixture in the 2nd stage has a composition of approx. 10 vol% CO2in H2. Thus, the data set for the 10 vol% CO2in H2listed in Table 3 was used for the 2nd- stage simulation.

Fig. 6 shows the effect of the 2nd-stage operating temperature on

membrane area (a), the power consumption (b), and CRC, OPEX, spe-

cific cost of H2purification (c). As can be seen, the membrane area of the

1st-stage is almost constant with increasing 2nd-stage temperatures, but

the  effect  on  the  2nd-stage membrane  area  is  significant,  showing  a

notable declining trend with increasing temperature, which is opposite

to the trend of the membrane area with the increasing 1st-stage tem-

perature. The opposite effects of temperature on CO2  permeance using

the feeds of 10 vol% CO2  in H2  and 40 vol% CO2  in H2  are believed to

have caused different trends. For the feed stream of 10 vol% CO2 in H2,

the  CO2   permeance  increases  with  increasing  temperature;  hence  a

higher CO2 flow goes through the membrane, leading to increasing en-

ergy consumption for both the vacuum pump at the permeate side in the

2nd-stage  and  the  compressor  to  pressurize  the  increasing  recycle

stream back to 1 bar to mix with the outlet stream of dark fermentation.

Thus, the power consumption of the process increases with increasing

2nd-stage temperature, as presented in Fig. 6 (b). As mentioned before,

the cost of membrane units and compressors dominates CRC. Thus, as

shown in Fig. 6 (c), the CRC cost decreases and OPEX increases (from

0.216 × 106 $ to 0.335 × 106 $) with increasing 2nd-stage temperature

due to the increase in power consumption.

Similarly, when the operating temperature of 2nd-stage increases, the specific cost of H2  purification also decreases, but it can be mini- mized by balancing CRC and OPEX. Based on these factors as discussed above, the optimal feed temperature of 2nd-stage is determined to be 55 ◦ C, which reaches the minimum H2specific purification cost of 0.156 $/Nm3. Surprisingly, the CO2  loss under the optimal condition is only 0.67 %, and CO2  purity has already been around 87 vol% (dry base). Thus, the two-stage CO2-selective membrane system designed for bio- hydrogen purification has a huge potential to obtain high purity of CO2 as a side-product. The data on effects of flow rate, operating tempera- ture, and H2 purification cost in Scenario A1 and A2 are provided in the Supporting information in Table S1.

4.2.3.  Three-stage membrane process simulation

Processes with two-stage configurations are the most commonly used multi-stage processes, as the complexity of variable control and the extra

图4.在25 ◦ C 、1.7 bar条件下，H2损失对单级膜工艺中膜面积（蓝线）及H2纯度与H2损失之间权衡（棕线）的影响。

在单级膜系统中，H2纯度达到要求，但生物氢纯化还需再增加一个阶段，才能达到所需的高纯度H2（99.5 vol%）和低H2损失（<10%）。

#### 4.2.2.   两段式膜工艺

由于操作温度显著影响PVAm/(PVA-GO)膜的气体分离性能，这必然进一步影响H2净化过程的资本成本和单位成本。因此，通过工艺模拟和经济性分析，在固定H2损失和H2纯度的前提下，对各膜单元的操作温度进行优化。根据含40 vol% CO2的H2进料气体实验数据，较高的操作温度会导致CO2渗透率降低， 同时选择性也会下降。 由于低CO2渗透率的膜会导致为满足H2纯度要求而增加所需的膜面积，因此需要额外的膜面积来补偿渗透率损失。因此， 由膜模块成本决定的CRC成为操作温度的函数。故可优化膜单元的操作温度， 以最小化H2净化的资本成本和单位成本。

本研究针对设计的两段式CO2选择性膜工艺（标记为情景A），系统分析了操作温度对膜面积、能耗及成本的影响 。设定总氢气损失率为10% 、H2纯度为99.5体积%（干基）为优化目标，仅允许第二阶段温度进行调整。表5详细列出了两段式膜系统中膜单元操作温度优化的方案：在A1方案中，第二阶段温度固定为25 ℃ , 允许第一阶段膜温度变化以优化其温度；而在A2方案中，基于A1方案优化的第一阶段温度将被固定， 以此研究第二阶段膜模块温度变化的影响。

当第一级膜的进料流温度从25 ◦ C升至75 ◦ C时，该工艺可轻松实施，因为

黑暗发酵的发酵温度为25 ◦ C至75 ◦ C（Lee 等，2011）。

当第一级操作温度升高时，第一级膜面积会轻微变化：在55 ◦ C时先减小后增大，而第二级膜面积则显著且近乎线性地增加。 由于膜的CO2渗透率随温度升高而增加，同时CO2/H2选择性降低，因此操作温度对第一级膜单元的膜面积具有显著影响 。不过第一级膜面积还受循环流影响——提高第一级膜单元的操作温度会增加所需的循环流比例，从而增大膜面积。这两种效应叠加后，第一级膜面积随温度呈现轻微的曲线下降趋势，但由于需要更大流量的循环流来满足H2纯度要求和H2损耗，整体能耗仍呈单调上升趋势，如图5(a)和(b)所示。 由于膜单元成本主导了CRC ，因此CRC值达到最小值，H2生产的比成本也呈现相同趋势，如图5 (c)所示。因此，第一阶段进料流的最佳操作温度设定为25 ◦ C ，该温度下纯化H2的比成本为0.266$/Nm3。

在确定第一级最佳进料流温度为25 ◦ C后，通过工艺模拟研究了第二级操作温度的影响，其中第一级温度固定为25 ◦ C ，第二级温度在25~75 ◦ C范围内变化，作为情景A2 。需要指出的是，第二级进料气混合物的组成约为10 vol% CO2in H2 。因此，表3中列出的10 vol% CO2in H2数据集被用于第二级模拟。

图6展示 了第 二 阶段操作温度对膜面积(a) 、 能耗(b) 以及CRC 、 OPEX 、H2净化特定成本(c)的影响。可以看出，第一阶段的膜面积随第二阶段温度升高几乎保持不变，但第二阶段膜面积受温度影响显著，呈现随温度升高而明显下降的趋势，这与第一阶段膜面积随温度升高而增加的趋势相反。使用10 vol%CO2在H2 中和40 vol%CO2在H2 中作为进料时，温度对CO2渗透率的相反影响被认为是导致不同趋势的原因。对于10 vol% CO2在H2中的进料流，CO2渗透率随温度升高而增加； 因此通过膜的CO2流量增加，导致第二阶段渗透侧真空泵和将增大的循环流加压至1bar以与暗发酵出口流混合的压缩机能耗均增加。因此，如图6(b)所示，随着第二级温度的升高，该工艺的功耗也随之增加。如前所述，膜单元和压缩机的成本主导了CRC的运行成本。因此，如图6(c)所示， 由于功耗的增加， 随着第二级温度的升高，CRC成本降低而 OPEX 增加（从0.216×106美元增至0.335×106美元）。

同样地，当第二级操作温度升高时，H2纯化的单位成本也会降低，但可通过平衡CRC和 OPEX 来最小化。基于上述讨论的这些因素，第二级的最佳进料温度被确定为55 ◦ C ， 此时H2 单位纯化成本达到最低值0. 156$/Nm3 。令人惊讶的是，在最佳条件下CO2损失仅为0.67% ，且CO2纯度已接近87 vol%（干基） 。因此，为生物制氢设计的两阶段CO2选择性膜系统具有获得高纯度CO2作为副产品的巨大潜力。情景A1和A2中关于流速、操作温度及H2纯化成本影响的数据详见支持信息中的表S1。

#### 4.2.3.   三段式膜工艺模拟

采用两阶段配置的工艺流程是最常用的多阶段工艺， 因其变量控制的复杂性及额外的

表5

膜单元操作温度优化的场景A。

| 场景 | T, ◦C 第一期 | T, ◦ C 第2 阶段 | Pfeed， bar | H2 纯 度 ，%（ 干基） | H2 损失率，% |
| --- | --- | --- | --- | --- | --- |
| A1 A2 | 25 ~ 75 优化 | 25 25 ~ 75 | 1.7 | 99.5 | 10 |

Fig. 5. Effects of the 1st-stage feed temperature on a) membrane area (orange line: 1st-stage, and green line: 2nd-stage), b) power consumption of major equipment, and c) CRC, OPEX, and specific cost.

Fig. 6.  Effects of 2nd-stage feed temperature on a) membrane area, b) power consumption of major equipment, and c) CRC, OPEX, and specific cost.

A 3rd-stage membrane unit was introduced to the optimized two- stage membrane processes to further purify the enriched CO2  from the permeate stream of the 1st-stage membrane to meet the CO2 capture specification. As shown in Fig. 7, three-stage membrane processes were designed. The potential of two different types of membrane in the added 3rd-stage, i.e., CO2-selective membranes as Scenario B (Fig. 4 (a)) and H2-selective membranes as Scenario C (Fig. 4 (b)), were investigated to find the most economical process design.

The same PVAm/(PVA-GO) membrane was used as the CO2-selective

membrane  in  the  3rd-stage  unit  as  Scenario  B.  Since  the  1st-stage

permeate stream feeding into the  3rd-stage membrane module has a

very  high  CO2   concentration  already,  the  permeation  of  the  large

amount oCO2                                 afwillrequire large membrane area. Thus, using an H2-

selective  membrane  in  the  3rd  stage  instead  could  be  a  promising

alternative considering the very low H2 content in the feed to that stage,

requiring a lower membrane area to permeate a smaller amount of H2.

In  the  case  of using  an  H2-selective  membrane  as  the  3rd  stage

membrane  (Scenario  C), several different types of H2-selective mem-

branes were compared by literature study to determine the most suitable

candidate  for  efficient  H2/CO2   separation  (Al-Rowaili  et  al.,  2023;

Cardoso et al., 2018; Sazali, 2020). According to the literature, Palla- dium (Pd)-based membranes have been widely investigated and known as  highly  H2   selective  (Atsonios  et  al.,  2014).  However,  Pd-based membranes are costly both for the materials and fabrication process. Besides, the low temperature and pressure for biohydrogen purification

costs limit the applications of processes with processes of three or more stages unless the additional stages result in significant benefits. Never- theless, adding an extra stage can further purify CO2 from the 2nd-stage H2 purification process as a by-product, which could be rewarding both economically and from the environmental perspective, i.e., achieving negative carbon emissions. In general, CO2 capture requires the process to meet specifications for CO2 storage or utilization, e.g., CO2 purity of > 90% and CO2capture rate of 90%, and the price of CO2 depends on its purity. Higher CO2  purity usually makes more value, thus selling at a higher price.

make H2 hard to dissociate, causing low diffusivity and, thus, low sep-

aration efficiency. The complicated impurities from the bioreactor may

poison Pd-membranes.aswell Therefore,  the  Pd  membrane  was  not

selected in this work. Carbon membrane has also been reported for their

high H2/CO2  selectivities (Tseng et al., 2016). Recently, Dai et al. (Dai

et al., 2023) and Lei et al. (Lei et al., 2021) reported H2-selective carbon

membranes with high H2/CO2selectivity, and Lei et al. have also studied

the  process  for  H2   purification.  Although  the  fabrication  of  carbon

membranes  is,  in  general,  costly,  Lei,s  study  showed  relatively  low

specific cost in processes for H2 purification by assuming the membrane

cost of 100$/m2 (Chen et al., 2023; He et al., 2021; Lei et al., 2021). It is

interesting to compare these studies with our work. Thus, the H2-se-

lective  cellulose-based  carbon  membrane  reported  by  Lei  et  al.  was

chosen as the 3rd-stage membrane unit in the current study.

As shown in Fig. 7 (a), a 3rd-stage CO2-selective membrane unit was set up for the process as Scenario B, in which the retentate stream out of the 1st-stage membrane unit (M − 1) is fed into the2nd-stage membrane unit (M − 2) to enrich H2  as the product, and the permeate stream from the 2nd-stage was recycled to M1 to ensure low H2 loss. The permeate side of M − 1 is fed into the 3rd-stage membrane unit (M − 3) with an additional compressor to increase the pressure to the 3rd-stage separa- tion pressure. M − 3 was used to enrich CO2 as the second product in the permeate, while the retentate stream was recycled to ensure low H2loss. The design is different in Scenario C (seeFig. 7 (b)), where the 1st-stage membrane unit (M − 1) and the 2nd-stage membrane unit (M − 2) are the same, but additional condenser (C-1) before the stream feeding into the 3rd-stage membrane unit (M − 3) was needed in order to remove water as water may cause a negative effect for carbon-based membranes gov- erned by the molecular sieving mechanism. Also, enriched CO2  is ob- tained  at the retentate  side of M − 3,  and the permeate  side must be recycled back to M1 to avoid H2  loss. Due to the requirement of high purity H2and only a small amount of CO2in the retentate side in M2, the resulting CO2  driving force is low at the 2nd-stage; thus, the 1st-stage was used to control the CO2  concentration in the fed of the 2nd-stage based on  = 0.5 (Mulder and Mulder,  1996). Adjust units (ADJ-1

图5.一级进料温度对以下指标的影响：a) 膜面积（橙色线：一级，绿色线：二级），b) 主要设备能耗，以及c) CRC 、 OPEX 和单位成本。

图6.二段进料温度对a)膜面积、b)主要设备能耗、c)循环比、 OPEX 及单位成本的影响。

成本限制了多阶段工艺的应用，除非新增阶段能带来显著效益。不过，作为副产品在第二阶段氢气提纯过程中额外增加一个阶段，可进一步提纯二氧化碳，这在经济和环保层面都具有双重优势——即实现负碳排放。通常而言，二氧化碳捕集工艺需满足二氧化碳储存或利用的规格要求，例如二氧化碳纯度需>90%且捕集率达90% ，而二氧化碳价格取决于其纯度。纯度越高价值越大，因此售价也越高。

为满足二氧化碳捕集规格要求，将第三阶段膜单元引入优化后的两阶段膜工艺流程， 以进一步从第一阶段膜的渗透物流中纯化富集的CO2 。如图7所示，设计了三阶段膜工艺流程。为寻找最具经济效益的工艺设计，研究了新增第三阶段中两种不同类型膜的潜力，即情景B（图4(a)）的CO2选择性膜和情景C（图4(b)）的H2选择性膜。

在情景B的第三级装置中，我们继续使用相同的PVAm/(PVA-GO)膜作为二氧化碳选择性膜。 由于进入第三级膜组件的第一级渗透物流中二氧化碳浓度本就极高，要让大量二氧化碳通过需要较大的膜面积。考虑到该阶段进料中氢气含量极低，采用氢气选择性膜作为第三级膜组件或许是个更优选择——这样既能降低膜面积需求，又能减少氢气的渗透量。

在使用H2选择性膜作为第三级膜的情况下（情景C），通过文献研究比较了多种不同类型的H2选择性膜， 以确定最适用于高效H2/CO2分离的 候 选 膜 （Al-Rowaili  等 人 ，2023；Cardoso  等 人 ，2018； Sazali ， 2020） 。根据文献，钯（Pd）基膜已被广泛研究，并被认为具有高度H2选择性（Atsonios 等人，2014） 。然而，Pd基膜在材料和制造工艺方面成本较高。此外，生物氢纯化所需的低温和低压

使H2难以解离，导致扩散性低，从而分离效率低下。生物反应器中的复杂杂质也可能毒害钯膜。因此，本研究未选择钯膜。碳膜因其高H2/CO2选择性也已被报道（Tseng 等人，2016） 。近期，Dai等人（Dai等人， 2023）和Lei等人（Lei 等人，2021）报道了具有高H2/CO2选择性的H2选择性碳膜，Lei等人还研究了H2纯化工艺。尽管碳膜的制备通常成本较高，但Lei的研究假设膜成本为100美元/平方米，表明H2纯化工艺的单位成 本 相 对 较 低 （Chen  等 人 ，2023； He  等 人 ，2021； Lei  等 人 ， 2021） 。将这些研究与我们的工作进行比较很有意义。因此，本研究选择Lei等人报道的H2选择性纤维素基碳膜作为第三阶段膜单元。

如图7(a)所示，该工艺采用第三级CO2选择性膜单元作为方案B ，其中第一级膜单元(M-1)的截留物流被送入第二级膜单元(M-2)以富集H2作为产物，第二级的渗透物流则循环回M1以确保低H2损失。M-1的渗透侧通过额外压缩机送入第三级膜单元(M-3) ，将压力提升至第三级分离压力。M-3用于在渗透物流中富集CO2作为第二产物， 同时截留物流循环回流以确保低H2损失。方案C的设计则不同（参见图7(b)），其第一级膜单元(M-1)与第二级膜单元(M-2)相同，但需在进入第三级膜单元(M-3)的物流前增设冷凝器(C-1) ， 以去除可能对基于分子筛机制的碳基膜产生负面影响的水分。此外，在M-3的截留侧获得富集的CO2 ，而渗透侧必须循环回M1以避免H2损失。 由于M2截留侧需要高纯度H2且仅含少量CO 2 ，第二阶段产生的CO2驱动力较低；因此，第一阶段用于控制第二阶段进料中CO2的浓度，基于 = 0.5（Mulder 和 Mulder ，1996） 。调整单位（ADJ-1）

Fig. 7. Process flow diagram of three-stage membrane systems using a) CO2-selective membrane (Scenario B) and b) using H2-selective membrane as the 3rd-stage for biohydrogen purification (Scenario C).

and  ADJ-2)  were  used  to  control  H2   purity  and  CO2   purity  as  the adjusted variable, respectively, and membrane area was adjusted as the target variable. Due to the extra preparation procedure for carbonization compared with polymeric membranes, 100 $/m2 is assumed as the price of cellulose-based carbon membranes, including materials and modules

of membranes and installation cost, the same value as given in (He et al., 2021; Lei et al., 2021).

To further investigate the feasibility of simultaneous CO2 capture in the  H2   purification  process,  the  proposed  scenarios  B  and  C  were modelled based on the optimal condition of the two-stage system. The

图7.采用a)CO2选择性膜（情景B）和b) 采用H2选择性膜作为第三阶段生物氢纯化（情景C）的三阶段膜系统工艺流程图。

实验中采用ADJ-2等试剂分别控制H2纯度和CO2纯度作为调整变量，膜面积则作为目标变量进行调整。 由于碳化处理比聚合物膜需要额外工序，纤维素基碳膜（含材料及组件）的单价设定为100美元/平方米。

膜和安装成本，与（He 等人，2021； Lei 等人，2021） 中给出的数值相同。

为进一步研究在H2纯化过程中同步捕集CO2的可行性，基于两段式系统的最优条件对提出的方案B和C进行了建模。

techno-economic analysis for the target H2 purity and H2 loss, and CO2 purity and CO2loss of the 3rd-stage were analyzed, as listed in Table 6, with the 1st-stage and 2nd-stage operating temperature set as 25 ◦ C and 55 ◦ C, respectively. Two different designs for scenarios B and C were compared, and the influence of different 3rd-stage membrane materials and operating temperatures were also investigated.

CO2-selective membrane in the 3rd-stage (Scenario B)

By using a CO2-selective membrane as the 3rd-stage, the 40 vol% CO2in H2data in Table 3 was used for simulation. As shown in Fig. 8 (a), the total membrane area shows a small difference at various tempera- tures at the 3rd-stage. According to the data for 40 vol% CO2 in H2, the CO2  permeance decrease, and H2  permeance increase with increasing operating temperature. Thus, to obtain high purity CO2in the 3rd-stage, a lower temperature is more favorable; Thus, a lower gas volume from the 3rd-stage retentate needs to be recycled due to the higher selectivity at a lower temperature (i.e., at 25 ◦ C), which, in turn, results in lower power consumption for the compressor and vacuum pump, as presented in Fig. 8(b).

Since power consumption dominates OPEX, the operating tempera- ture (feed flow temperature) can be optimized by tuning the optimal operation  temperatures  to  minimize  the  specific  cost.  Fig.  9  demon- strates the effect of the 3rd-stage feed temperature on CRC, OPEX, and specific cost. Due to the slight increase in membrane area and power consumption, the CRC and OPEX increase slightly, and consequently, the specific cost of H2  purification follows the same trend. Thus, the optimal specific cost of purifying 99.5 vol% H2  (≪10% H2 loss) and 90 vol% CO2(<1% CO2loss) is 0.189 $ per Nm3 of purified hydrogen when the 3rd-stage operating at the optimal temperature of 45 ◦ C, or roughly in the range of 35-55 ◦ C. Moreover, if the carbon credit income of the captured CO2  as a by-product of hydrogen production is available and included, the hydrogen purification cost could be even lower.

H2-selective membrane in the 3rd-stage (Scenario C)

By  using  an  H2-selective  membrane  as  the  3rd  stage,  a  carbon membrane based on the data given in Table 4 was applied to investigate the temperature influence. The data, such as flow rate, operating tem- perature, and H2 purification cost of Scenario B and C, are summarized in the Supporting Information in Table S2. One of the advantages of cellulose-based carbon membranes is that both H2/CO2  selectivity and H2   and  CO2   permeance  increase  with  increasing  temperature.  The analysis  of  the  operating  temperature  over  an  expanded  range  of 25-75 ◦ C was investigated in order to obtain a relatively high purity of CO2  (90 vol%, dry base) with low H2  loss and CO2  loss. As shown in Fig. 10 (a), membrane areas of the 1st-stage and 2nd-stage are almost constant, and the membrane area of the 3rd-stage slightly decreases with increasing   3rd-stage   operating   temperature   since   H2     permeance increased and less membrane area is needed to obtain the requirement of CO2 purity. More energy may be needed for a large amount of recycling for the permeate of the 3rd-stage. Nevertheless, according to the simu- lation, the increased total power consumption is negligible, and hence the influence of the 3rd-stage temperature on OPEX can be neglected, as shown in Fig. 10 (b) for the CRC, OPEX, and specific cost plots. CRC has shown a small decrease with increasing operating temperature, causing a slightly decreasing specific cost for H2 purification. Based on the fac- tors, under 75 ◦ C, the specific cost for H2 purification reaches the lowest value at 0.173 $/Nm3  if the heating and water removal costs are not included. Compared with using a CO2-selective membrane as the 3rd- stage membrane system, using an H2-selective membrane gives only a

little lower specific cost for purifying H2, but with only a<10% differ- ence for this case when the CO2  purity is set to be 90%. Taking into account the pre-treatment steps needed when using a carbon membrane, there is no benefit to changing the 3rd-stage membrane to an H2-se- lective carbon membrane when the targeted CO2 purity is only 90%.

It  is worth mentioning  that  current biohydrogen processes  are  at relatively small scales. In order to be close to the real industrial condi- tion, a relatively low total feed flow (gas stream from dark fermentation) was used in these simulations for fermentative hydrogen purification. Therefore,  the vacuum  pump  sizes  are  too  small  to  use  rotary  com- pressors in CAPEX estimation, so the selling price of SMC Vacuum Pump from RS Norway (~770 $/piece) was used to calculate the CAPEX based on the Eq. (3).

4.3.  Sensitivity analysis of CO2 purity in the three-stage process

Based on the above optimized operating temperature for the three- stage membrane separation system, the sensitivity analysis of the ef- fects ofCO2purity as different products (90-99.95%) was analyzed with fixed H2purity (99.5 vol%), H2loss < 10 %, and CO2loss < 1 %, as listed in Table 6 marked with a star (*). Since scenarios B and C show similar specific costs (<10% difference), the sensitivity analysis of CO2  purity with a CO2-selective membrane as the 3rd-stage membrane or an H2- selective membrane as the 3rd-stage membrane should be investigated. Since  the  selectivity  of  CO2/H2   in  the  CO2-selectivemembrane  is limited, according to a preliminary study, achieving a higher CO2 purity of  > 95%  using  the  CO2-selective  membrane  as  the  3rd-stage  is  too costly. Thus,  only  using  the  H2-selective  membrane  in  the  3rd  stage (scenario  C*) was  investigated  on  the  techno-economic  feasibility  of obtaining CO2of different purities as side products.

Fig. 11 summarizes the sensitivity of the required CO2 purity on the process design. As shown in Fig. 11 (a), when increasing the operating temperature of the 3rd-stage from 25 to 75 ◦ C, the total membrane area slightly decreases, from 82 600 to 79 600 m2 for 90 vol% CO2purity and from 98 800 to 88 300 m2  for 95vol% CO2 purity. High CO2 purity of 99.5% and above requires a much larger membrane area. According to the  carbon  membrane,s  gas  separation  performance  (see  Table  4), increasing temperature leads to the increase of both gas permeances and H2/CO2  selectivity. Therefore, increasing the operating temperature of the 3rd stage decreases the 3rd-stage and total membrane area, which directly  reduces  CRC,  as  shown  in  Fig.  11  (b).  Since  OPEX  is  only considered the influence of electricity and labor cost in this work, and in the sensitivity analysis, the differences in power consumption on each concentration with different temperatures are small, the OPEX differ- ence can be neglected in the analysis. Fig. 11 (c) shows the specific cost for H2 purification increases for producing high-purity CO2.

5.  Conclusions

A two-stage membrane system was designed using a CO2-selective membrane (PVAm/(PVA-GO)) to obtain high-purity H2  as high-quality biofuel  from  biomass  through  dark  fermentation.  According  to  the simulation results, using the PVAm/PVA-GO membrane for biohydrogen purification is economically feasible; Only ~ 0.156 $ is needed for the purification  of each Nm3  of biohydrogen  to reach  99.5 vol%  purity, leaving CO2  (~87%) as a by-product.

To further purify CO2 to meet the CO2 capture specification for CO2

Table 6

Simulation parameters for scenario B and C.

| Scenario | Membrane type | 1st-stage | T, ◦C 2nd-stage | 3rd-stage | H2 purity, % | H2 loss, % | CO2 purity, % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| B C | CO2-selective H2-selective | 25 | 55 | 25-75 | 99.5 | <10 | 90 (90-99.5)* |

*Data used for sensitivity study of CO2 purities.

针对目标H2纯度和H2损失， 以及第三级CO2纯度和CO2损失进行了技术经济分析，如表6所示，第一级和第二级操作温度分别设定为25 ◦ C和55 ◦ C 。 比较了情景B和C的两种不同设计方案，并研究了不同第三级膜材料和操作温度的影响。

第三阶段的CO2选择性膜（情景B）

通过使用CO2选择性膜作为第三级，采用表3中40 vol% CO2在H2中的数据进行模拟。如图8(a)所示，第三级在不同温度下的总膜面积存在微小差异。根据40 vol%CO2在H2中的数据，CO2渗透率随操作温度升高而降低，H2渗透率则随之增加。因此，为在第三级获得高纯度CO2 ，较低温度更为有利； 由于较低温度（即25 ◦ C）下具有更高的选择性，第三级截留气体中需要循环的气体体积更少，这进而降低了压缩机和真空泵的能耗，如图8(b)所示。

由于功耗主导 OPEX ，通过调节最佳运行温度以最小化单位成本，可优化操作温度（进料流温度） 。图9展示了第三级进料温度对CRC 、 OPEX 及单位成本的影响 。 由于膜面积和功耗的轻微增加 ，CRC 和OPEX 略有上升，因此H2净化的单位成本呈现相同趋势。因此，当第三级在45 ◦ C的最佳温度下运行时（约35-55 ◦ C范围内），净化99.5 vol%H2 （垣10%H2损失）和90 vol% CO2（<1% CO2损失）的最优单位成本为每Nm3净化氢气0. 189美元。此外，若将捕获CO2作为制氢副产品产生的碳信用收入纳入考量，氢气净化成本可进一步降低。

第三阶段的H2选择性膜（情景C）

通过使用H2选择性膜作为第三阶段，基于表4中给出的数据，应用碳膜来研究温度影响。情景B和C的流量、操作温度以及H2纯化成本等数据汇总于表S2的支持信息中。纤维素基碳膜的一个优势是，其H2/CO2选择性和H2与CO2渗透率均随温度升高而增加。为获得相对较高的CO2纯度（90体积% ，干基）且H2损失和CO2损失较低，对25-75 ◦ C扩展范围内的操作温度进行了分析。如图10(a)所示，第一阶段和第二阶段的膜面积基本保持不变，而第三阶段的膜面积随其操作温度升高略有减小，因为H 2渗透率增加，且获得CO2纯度要求所需的膜面积减少。对于第三级渗透液的大规模循环可能需要更多能量。然而根据模拟结果，总能耗的增加可以忽略不计，因此第三级温度对 OPEX 的影响可以忽略，如图10(b)中CRC 、 OPEX 和比成本曲线所示。CRC随操作温度升高略有下降，导致H2提纯的比成本略有降低。基于这些因素，在75 ◦ C以下，若不计入加热和脱水成本，H2提纯的比成本在0. 173$/Nm3时达到最低值。与使用CO2选择性膜作为第三级膜系统相比，使用H2选择性膜仅能

净化H2的特定成本略低，但当CO2纯度设定为90%时，此情况下的差异仅为<10% 。考虑到使用碳膜时所需的预处理步骤，当目标CO2纯度仅为90%时，将第三阶段膜更换为H2选择性碳膜并无益处。

值得一提的是，当前的生物氢工艺规模相对较小。为了更接近实际工业条件，这些模拟中采用了相对较低的总进料流量（来自暗发酵的气体流）来进行发酵氢纯化。 因此，真空泵的尺寸太小，无法在 CAPEX估算中使用旋转压缩机，所以采用了RS Norway的SMC真空泵（约770美元/件）的售价，基于等式(3)计算 CAPEX 。

### 4.3.   三阶段工艺中二氧化碳纯度的敏感性分析

基于上述优化后的三阶段膜分离系统操作温度，我们以固定氢气纯度（99.5 vol%）、氢气损失率<10% 、二氧化碳损失率<1%为条件（如表6中带星号标注的方案），对不同产品（90-99.95%）的二氧化碳纯度影响进行了灵敏度分析。 由于方案B和C的特定成本差异较小（<10%），需要进一步研究采用二氧化碳选择性膜或氢气选择性膜作为第三阶段膜时，二氧化碳纯度的敏感性。根据初步研究， 由于二氧化碳选择性膜对二氧化碳/氢气的选择性有限，若采用该膜作为第三阶段膜，要实现> 95%的二氧化碳纯度成本过高。因此，我们仅针对第三阶段采用氢气选择性膜（方案C*） 的情况，研究了获取不同纯度二氧化碳作为副产品的技术经济可行性。

图11总结了所需CO2纯度对工艺设计的敏感性。如图11(a)所示，当第三级操作温度从25升至75 ◦ C时，总膜面积略有减小：对于90 vol% CO2纯度从82 600降至79 600 m2 ，对于95 vol%CO2纯度从98 800降至88 300 m 2 。99.5%及以上的高CO2纯度需要更大的膜面积。根据碳膜的气体分离性能（见表4），温度升高会导致气体渗透率和H2/CO2选择性同时增加。因此，提高第三级操作温度会减小第三级膜面积和总膜面积，从而直接降低CRC ，如图11(b)所示。 由于本研究仅考虑 OPEX 对电力和人工成本的影响，且在敏感性分析中不同温度下各浓度的能耗差异较小， OPEX 差异在分析中可忽略。图11(c)显示了H2的特定成本尿素化程度增加以生产高纯度CO2。

## 5.   结论

本研究采用CO2选择性膜（PVAm/(PVA-GO)） 设计了两阶段膜系统，通过暗发酵工艺从生物质中制取高纯度H2作为优质生物燃料。模拟结果显示，使用PVAm/PVA-GO膜进行生物氢提纯具有经济可行性：每生产1Nm 3 生物氢，仅需约0. 156美元即可达到99.5体积%的纯度， 同时将CO2（约87%）作为副产物排出。

为了进一步净化CO2以满足CO2捕获规范的要求CO2

表6

情景B与C的模拟参数。

| 场景 | 膜型 | 第一期 | T ，◦ C 第二阶段 | 第三期 | H2纯度，% | H2损失，% | CO2纯度，% |
| --- | --- | --- | --- | --- | --- | --- | --- |
| B C | CO2-选择性H2选择性 | 25 | 55 | 25-75 | 99.5 | <10 | 90 (90-99.5)* |

*用于CO2纯度敏感性研究的数据。

Fig. 8. Effects of 3rd-stage feed temperature on the a) membrane area (CO2-selective) and b) power consumption of major equipment.

Fig. 9.  Effects of 3rd-stage (CO2-selective) feed temperature on CRC, OPEX and specific cost.

Fig. 10. Effects of 3rd-stage (H2-selective) feed temperature on a) membrane area and power consumption, and b) CRC, OPEX and specific cost of producing H2.

图8.第三阶段进料温度对a)膜面积（CO2选择性）和b)主要设备功耗的影响。

图9.第三阶段（CO2选择性）进料温度对CRC 、 OPEX 和特定成本的影响。

图10.第三阶段（H2选择性）进料温度对a)膜面积和功耗，以及b)生产H2 的CRC 、 OPEX 和单位成本的影响。

Fig. 11. Sensitivity analysis of CO2  purity on a) membrane area, b) CRC, and c) specific cost of H2  production in scenario C*.

storage or utilization and achieve negative carbon emission, a 3rd-stage membrane was introduced to the two-stage process using either a CO2- selective membrane unit (scenario B) or an H2-selective membrane as the 3rd-stage (scenario C and C*), with which CO2capture with different purities for storage or various utilization applications can be achieved at a low cost. In the three-stage process, the specific cost for H2purification can take in the selling income of two products, H2  and CO2, and the selling  price  of the  higher  purity  of  CO2   also  increases,  which  will partially offset the increased production cost. As the selling profits of H2 as high quality fuel and high purity CO2with different applications were not included in this work, the actual profit was underestimated.

Cardoso, S.P., Azenha, I.S., Lin, Z., Portugal, I., Rodrigues, A.E., Silva, C.M., 2018.

In future work, costs for the pre-treatment steps in using H2-selective carbon membranes must be added to the process design and economic analysis, and amore detailed economic analysis and cash flow should be conducted by  taking  into  account  the  CO2  income when  the  market prices of CO2at various purities are available. Applying membranes with improved performance may result in a lower capital cost, such as using our recently reported H2-selective carbon membrane with superior CO2/ H2 separation performance (Dai et al., 2023).

CRediT authorship contribution statement

Wenqi Xu: Methodology, Formal analysis, Validation, Investigation, Writing – original draft, Visualization. Arne Lindbråthen: Writing – review & editing. Saravanan Janakiram: Writing – review & editing. Luca Ansaloni: Writing – review & editing, Funding acquisition. Lin- feng Lei: Writing – review & editing. Liyuan Deng: Conceptualization, Writing – review & editing, Supervision, Project administration, Fund- ing acquisition.

Declaration of Competing Interest

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

Data availability

Data will be made available on request.

Acknowledgements

This work is part of the FaT H2 project supported by the Research Council of Norway (No. 294533).

Appendix A.  Supplementary data

Experimental data of CO2 and H2 permeance and the simulation and economic data of Scenarioes A1, A2, B and C. Supplementary data to this article  can  be  found  online  at  https://doi.org/10.1016/j.ces.2023.11

9219.

References

Al-Rowaili, F.N., Khaled, M., Jamal, A., Zahid, U., 2023. Mixed matrix membranes for H2/CO2 gas separation- a critical review. Fuel 333, 126285.

Ansaloni, L., Zhao, Y.N., Jung, B.T., Ramasubramanian, K., Baschetti, M.G., Ho, W.S.W.,

2015. Facilitated transport membranes containing amino-functionalized multi-

walled carbon nanotubes for high-pressure CO2 separations. J. Membr. Sci. 490,

18–28.

Atsonios, K., Panopoulos, K., Doukelis, A., Koumanakos, A., Kakaras, E., Peters, T., van Delft, Y., 2014. Introduction to palladium membrane technology. Palladium

Membrane Technology for Hydrogen Production, Carbon Capture and Other

Applications: Principles, Energy Production and Other Applications. Elsevier, 1-21.

Bernardo, G., Araújo, T., da Silva Lopes, T., Sousa, J., Mendes, A., 2020. Recent advances

in membrane technologies for hydrogen purification. Int. J. Hydrogen Energy 45

(12), 7313–7338.

Inorganic Membranes for Hydrogen Separation. Sep. Purif. Rev. 47 (3), 229–266.

Cartwright, E.D., 2021. “Code Red”—Recent IPCC Report Warns Time is Running Out on

Climate Change. Climate Energy 38 (3), 11–12.

Chen, K.K., Han, Y., Tong, Z.i., Gasda, M., Ho, W.S.W., 2021. Membrane processes for

CO2 removal and fuel utilization enhancement for solid oxide fuel cells. J. Membr.

Sci. 620, 118846.

Chu, Y.H., Lindbrathen, A., Lei, L.F., He, X.Z., Hillestad, M., 2019. Mathematical

Chen, D., Wang, K., Yuan, Z., Lin, Z., Zhang, M., Li, Y., Tang, J., Liang, Z., Li, Y., Chen, L., Li, L., Huang, X., Pan, S., Zhu, Z., Hong, Z., He, X., 2023. Boosting membranes for CO2 capture toward industrial decarbonization. Carbon Capture Sci. Technol. 7,    100117.

modeling and process parametric study of CO2 removal from natural gas by hollow

fiber membranes. Chem. Eng. Res. Des. 148, 45–55.

Czyperek, M., Zapp, P., Bouwmeester, H.J.M., Modigell, M., Ebert, K., Voigt, I.,            Meulenberg, W.A., Singheiser, L., St¨over, D.,             G2010.as separation membranes for zero-emission fossil power plants: MEM-BRAIN. J. Membr. Sci. 359 (1-2), 149–159.

Dai, Z., Deng, J., Yu, Q., Helberg, R.M.L., Janakiram, S., Ansaloni, L., Deng, L., 2019.

Fabrication and Evaluation of Bio-Based Nanocomposite TFC Hollow Fiber

Membranes for Enhanced CO(2) Capture. ACS Appl. Mater. Interfaces 11 (11),

10874–10882.

Dai, Z., Guo, H., Deng, J., Deng, L., Yan, J., Spontak, R.J., 2023. Carbon molecular-sieve

membranes developed from a Tr¨oger s, base polymer and possessing superior gas-

separation performance. J.Membr. Sci. 680, 121731.

Deng, L., H¨agg, M.-B., 2010. Techno-economic evaluation of biogas upgrading process

using CO2 facilitated transport membrane. Int. J. Greenhouse Gas Control 4 (4), 638–646.

Franz, J., Scherer, V., 2010. An evaluation of CO2 and H2 selective polymeric

membranes for CO2 separation in IGCC processes. J. Membr. Sci. 359 (1-2),

173–183.

Ghimire, A., Frunzo, L., Pirozzi, F., Trably, E., Escudie, R., Lens, P.N.L., Esposito, G.,

2015. A review on dark fermentative biohydrogen production from organic biomass:

Process parameters and use of by-products. Appl. Energy 144, 73–95.

Guo, X.M., Trably, E., Latrille, E., Carre、re, H., Steyer, J.-P., 2010. Hydrogen production

from agricultural waste by dark fermentation: A review. Int. J. Hydrogen Energy 35

(19), 10660–10673.

H¨agg, M.-B., Deng, L., 2015. Membranes in gas separation, in: 2 (Ed.), Handbook of Membrane Separations: Chemical, Pharmaceutical, Food, and Biotechnological Applications. CRC press, pp. 143-180.

Han, Y., Ho, W.S.W., 2020. Recent advances in polymeric facilitated transport

membranes for carbon dioxide separation and hydrogen purification. J. Polym. Sci.

58 (18), 2435–2449.

Han, Y., Ho, W.S.W., 2021a. Facilitated transportmembranes for H2 purification from

coal-derived syngas: A techno-economic analysis. J. Membr. Sci. 636, 119549.

J. Membr. Sci. 628, 119244.

Han, Y., Ho, W.S.W., 2021b. Polymeric membranes for CO2 separation and capture.

图11.CO2纯度对a)膜面积、b) CRC以及c)情景C*中H2生产特定成本的敏感性分析。

为实现碳储存或利用并达成负碳排放目标，研究者在两阶段工艺中引入了第三阶段膜技术，采用CO₂选择性膜单元（情景B）或H₂选择性膜作为第三阶段（情景C和C*），从而以较低成本实现不同纯度CO₂ 的捕集以满足储存或多样化利用需求。在三阶段工艺中，H₂提纯的特定成本可抵消两种产品H₂和CO₂ 的销售收入，且高纯度CO₂ 的售价也有所提升，这将部分抵消生产成本的增加。 由于本研究未包含H₂作为优质燃料及不同应用的高纯度CO₂ 的销售利润，实际利润被低估。

在后续研究中，使用H₂选择性碳膜的预处理步骤成本必须纳入工艺设计与经济分析，当不同纯度CO₂市场价格可得时，应结合CO₂收入进行更详尽的经济分析与现金流测算。采用性能更优的膜材料可降低资本成本，例如使用我们近期报道的具有卓越CO₂/H₂分离性能的H₂选择性碳膜（Dai 等，2023）。

## CRediT作者贡献声明

徐文奇 ：方法论、形式分析、验证、调查、撰写初稿、可视化。阿恩·林德布拉滕 ：撰写、审阅与编辑。萨拉瓦南·贾纳基拉姆 ：撰写、审阅与编辑。卢卡·安萨洛尼 ：撰写、审阅与编辑、资金获取。雷林峰 ：撰写、审阅与编辑。邓丽媛 ：概念化、撰写、审阅与编辑、监督、项目管理、资金获取。

## 利益冲突声明

作者声明，其不存在任何已知的可能影响本文所报告工作的竞争性经济利益或个人关系。

## 数据可用性

数据将根据要求提供。

## 致谢

本研究为挪威研究理事会资助的FaT H2项目（编号：294533） 的一部分。

## 附录A. 补充数据

CO2和H2渗透率的实验数据以及情景A1 、A2 、B和C的模拟和经济数据。本文的补充数据可在https://doi.org/10.1016/j.ces.2023.11在线获取。

9219.

## 参考文献

Al-Rowaili ，F.N. ，Khaled ，M. ，Jamal ，A. ，Zahid ，U. ，2023. 混合基质膜用于H2/二氧化碳气体分离——一项关键性综述。Fuel 333, 126285 。

安萨洛尼，L. ，赵，Y.N. ，仲，B.T. ，拉马苏布拉马尼安，K. ，巴舍蒂，M.G. ，霍，W.S.

W.

2015年。含有氨基功能化多壁碳纳米管的促进传输膜用于高压二氧化碳分离。膜科学杂志 490 ，

18-28.

Atsonios ，K.  、 Panopoulos ，K.  、 Doukelis ，A.  、 Koumanakos ，A.  、 Kakaras ，E.  、 Peters ，T. 、van Delft ，Y. ，2014年。《钯膜技术导论》 。《钯膜技术在制氢、碳捕集及其他应用中的原理、能源生产及其他应用》 。爱思唯尔，1-21页。

Bernardo ，G. ，Araujo ，T. ，da Silva Lopes ，T. ，Sousa ，J. ，Mendes ，A. ，2020. 近期氢气

提纯膜技术进展. 国际氢能杂志 45

(12), 7313-7338.

卡多索，S.P. ，阿泽尼亚，I.S. ，林，Z. ，葡萄牙，I. ，罗德里格斯，A.E. ，西尔瓦，C.

M. ，2018.

用于氢分离的无机膜。分离纯化评论 47 (3) ，229-266 。

卡特赖特，E.D. ，2021年。《红色警报》——最新IPCC报告警告时间所剩无几

气候变化。气候能源 38 (3) ，11-12 。

Chen ，K.K. ，Han ，Y. ，Tong ，Z.i. ，Gasda ，M. ，Ho ，W.S.W. ，2021. 用于二氧化碳去除和固体氧化物燃料电池燃料利用增强的膜工艺. J. Membr.Sci. 620, 118846.

Chen，D.，Wang，K.，Yuan，Z.，Lin，Z.，Zhang，M.，Li，Y.，Tang，J.，Liang，

Z. ，Li ，Y. ，Chen ，L. ，Li ，L. ，Huang ，X. ，Pan ，S. ，Zhu ，Z. ，Hong ，Z. ，He ，

X.，2023. 提升膜技术 以二氧化碳捕集促进工业脱碳 。 碳捕集科 学 与技术 7， 100117。

Chu，Y.H.，Lindbrathen，A.，Lei，L.F.，He，X.Z.，Hillestad，M.，2019. 数学模型与中空纤维膜从天然气中去除二氧化碳的工艺参数研究. Chem. Eng. Res. Des. 148,45-55.

Czyperek，M.，Zapp，P.，Bouwmeester，H.J.M.，Modigell，M.，Ebert，K.，Voigt，I.， Meulenberg，W. A.，Singheiser，L.，Sto¨ver，D.，Gas        2010年，零排放化石发电厂分离膜：MEM-brain. J. Membr. Sci. 359 (1-2)，149-159。

Dai，Z. ，Deng，J. ，Yu，Q. ，Helberg，R.M.L. ，Janakiram，S. ，Ansaloni，L. ，

Deng ，L. ，2019.生物基纳米复合 TFC 中空纤维膜的制备与评估用于增强CO(2)捕

集. ACS应用材料与界面 11 (11)，10874-10882.

Dai，Z.，Guo，H.，Deng，J.，Deng，L.，Yan，J.，Spontak，R.J.，2023.   由 Tro	ger，s

碱性聚合物开发的具有优异气体分离性能的碳分子筛膜。J. Membr. Sci. 680, 121731。

邓，L.，哈¨gg，M.-B.          2010

process. 利用二氧化碳促进传输膜升级沼气的工艺经济性评估. 国际温室气体控制杂

志 4 (4) ，638-646.

Franz ，J. ，Scherer ，V. ，2010. 二氧化碳和H2选择性聚合物的评估

用于 IGCC 过程中二氧化碳分离的膜。《膜科学杂志》359卷（1-2期）

173-183.

吉米雷，A. ，弗伦佐，L. ，皮罗齐，F. ，特拉布利，E. ，埃斯库迪，R. ，伦斯，P.N.L. ，埃斯波西托，G.

2015年 有机生物质暗发酵生物产氢研究综述

工艺参数与副产物利用。应用能源 144,73-95 。

郭X.M. 、特拉布利E. 、拉特里尔E. 、卡雷H. 、斯泰尔J.-P. 、氢     2010.         通过暗发酵

从农业废弃物中生产：综述。国际氢能期刊 35

(19), 10660-10673.

Ha	gg ，M.-B. ， Deng ，L. ，2015年 。《气体分离中的膜技术》 ，载于：2（编），

《膜分离手册： 化学、制药、食品与生物技术应用》 。CRC出版社，第143-180

页。

韩Y 、何W.S.W. ，2020年。聚合物促进转运的最新进展

用于二氧化碳分离和氢气提纯的膜材料。《高分子科学杂志》

58 (18), 2435-2449.

韩Y. 、何W.S.W. ，2021a. 用于H2纯化的辅助转运膜

煤制合成气：一项技术经济分析。膜科学杂志 636, 119549 。

韩，Y. ，霍，W.S.W. ，2021b. 用于二氧化碳分离与捕获的聚合物膜。

J. Membr. Sci. 628, 119244.

Tong, Z., Ho, W.S.W., 2017. New sterically hindered polyvinylamine membranes for CO2 separation and capture. J. Membr. Sci. 543, 202-211.

He, X., Lei, L., Dai, Z., 2021. Green hydrogen enrichment with carbon membrane

276, 119346.

processes: Techno-economic feasibility and sensitivity analysis. Sep. Purif. Technol.

Huang, L., Xing, Z., Zhuang, X., Wei, J., Ma, Y., Wang, B., Jiang, X., He, X., Deng, L.,

Dai, Z., 2022. Polymeric membranes and their derivatives for H2/CH4 separation:

State of the art. Sep. Purif. Technol. 297, 121504.

Janakiram, S., Martín Espejo, J.L., Yu, X., Ansaloni, L., Deng, L., 2020. Facilitated

transport membranes containing graphene oxide-based nanoplatelets for CO2

separation: Effect of 2D filler properties. J. Membr. Sci. 616, 118626.

Lee,D.-J., Show, K.-Y., Su, A.y., 2011. Dark fermentation on biohydrogen production:

Pure culture. Bioresour. Technol. 102 (18), 8393-8402.

Lei, L., Lindbråthen, A., Hillestad, M., He, X., 2021. Carbon molecular sieve membranes

for hydrogen purification from a steam methane reforming process. J. Membr. Sci.

627, 119241.

Li, P.Y., Wang, Z., Qiao, Z.H., Liu, Y.N., Cao, X.C., Li, W., Wang, J.X., Wang, S.C., 2015.

Recent developments in membranes for efficient hydrogen purification. J. Membr.

Sci. 495, 130-168.

Lin, H., Van Wagner, E., Freeman, B.D., Toy, L.G., Gupta, R.P., 2006. Plasticization-

enhanced hydrogen purification using polymeric membranes. Science 311 (5761), 639-642.

Mulder, M., Mulder, J., 1996. Basic principles of membrane technology. Springer science

& businessmedia.

Nanda, S., Azargohar, R., Dalai, A.K., Kozinski, J.A., 2015. An assessment on the

sustainability of lignocellulosic biomass for biorefining.Renew. Sustain. Energy Rev.

50, 925-941.

Norahim, N., Yaisanga, P., Faungnawakij, K., Charinpanitkul, T., Klaysom, C., 2018.

Recent Membrane Developments for CO2 Separation and Capture. Chem. Eng.

Technol. 41, 211-223.

Pal, N., Agarwal, M., 2021. Advances in materials process and separation mechanism of

the membrane towards hydrogen separation. Int. J. Hydrogen Energy 46 (53), 27062-27087.

Rafiq, S., Deng, L., H¨agg, M.-B., 2016. Role of Facilitated Transport Membranes and Composite Membranes for Efficient CO2 Capture - A Review. ChemBioEng Rev. 3 (2), 68-85.

Rivero, J.R., Nemetz, L.R., Da Conceicao, M.M., Lipscomb, G., Hornbostel, K., 2023.

Modeling gas separation in flat sheet membrane modules: Impact of flow channel size variation. Carbon Capture Sci. Technol. 6, 100093.

Salleh, W., Ismail, A.F., 2015. Carbon membranes for gas separation processes: Recent

progress and future perspective. J. Membr. Sci. Res. 1, 2-15.

Sarangi, P.K., Nanda, S., 2020. Biohydrogen Production Through Dark Fermentation. Chem. Eng. Technol. 43 (4), 601-612.

Sazali, N., 2020. A Short Review on Separation of H2/CO2 usingPolymer Membrane.

J. Adv. Res. Fluid Mech. Therm. Sci. 69, 174-182.

Sazali, N., Mohamed, M.A., Salleh, W.N.W., 2020. Membranes for hydrogen separation: a

significant review. Int. J. Adv. Manuf. Technol. 107 (3-4), 1859-1881.

The Chemical Engineering                      Index -                  Engineering.PlantCostChemical

Tseng, H.-H., Wang, C.-T., Zhuang, G.-L., Uchytil, P., Reznickova, J., Setnickova, K.,

2016. Enhanced H2/CH4 and H2/CO2 separation by carbon molecular sieve

membrane coated on titania modified alumina support: Effects of TiO2 intermediate

layer preparation variables on interfacial adhesion. J. Membr. Sci. 510, 391-404.

Turton, R., Bailie, R.C., Whiting, W.B., Shaeiwitz, J.A., 2008. Analysis, synthesis and

design of chemical processes. Pearson Education.

separation by GO and PVA-GO embedded PVAm nanocomposite membranes.

J. Membr. Sci. 671, 121397.

Xu, W., Lindbråthen, A., Janakiram, S., Ansaloni, L., Deng, L., 2023. Enhanced CO2/H2

Yang, Y., Han, Y., Pang, R., Ho, W.S.W., 2020. Amine-Containing Membranes with

Functionalized Multi-Walled Carbon Nanotubes for CO2/H2 Separation. Membranes

(Basel) 10, 333.

Younas, M., Shafique, S., Hafeez, A., Javed, F., Rehman, F., 2022. AnOverview of

Hydrogen Production: Current Status, Potential, and Challenges. Fuel 316, 123317. Zhao, Y.N., Ho, W.S.W., 2012. Steric hindrance effect on amine demonstrated in solid

polymer membranes for CO2 transport. J. Membr. Sci. 415, 132-138.

Zhao, Y., Jung, B.T., Ansaloni, L., Ho, W.W., 2014. Multiwalled carbon nanotube mixed

matrix membranes containing amines for high pressure CO2/H2 separation.

J. Membr. Sci. 459, 233-243.

何X 、雷L 、戴Z ，2021 。碳膜富集绿色氢气

工艺流程：技术经济可行性与敏感性分析。纯化技术。

276, 119346.

黄立、邢志、庄旭、魏杰、马勇、王斌、姜晓、何晓、邓立

戴Z. ，2022年。用于H2/甲烷分离的聚合物膜及其衍生物：

国际权威期刊。《纯化技术》297卷，121504页。

Janakiram ，S. ，Martin Espejo ，J.L. ，Yu ，X. ，Ansaloni ，L. ，Deng ，L. ，2020. 含氧化石

墨烯纳米片的促进CO传输膜2

分离：二维填料特性的影响。膜科学杂志 616, 118626 。

Lee ，D.-J. ，Show ，K.-Y. ，Su ，A.y. ，2011. 黑色发酵在生物氢生产中的应用：

纯培养。生物资源与技术。102(18) ，8393-8402 。

雷，L. ，林德布拉森，A. ，希尔施塔德，M. ，何，X. ，2021. 碳分子筛膜

用于蒸汽甲烷重整过程中的氢气提纯。《膜科学杂志》

627, 119241.

李，P.Y. ，王，Z. ，郭，Z.H. ，刘，Y.N. ，曹，X.C. ，李，W. ，王，J.X. ，王，S.C. ，

2015.

高效氢气纯化膜的最新进展。膜科学杂志。

Sci. 495, 130-168.

林H 、范·瓦格纳E 、弗里曼B.D. 、托伊L.G. 、古普塔R.P. ，2006 。增塑作用-

采用聚合物膜增强氢气纯化。Science 311 (5761) ，639-642。

Mulder ，M. ，Mulder ，J. ，1996. 膜技术基础原理. 斯普林格科学出版社

和商业媒体。

Nanda ，S. ，Azargohar ，R. ，Dalai ，A.K. ，Kozinski ，J. A. ，2015. 一项评估

木质纤维素生物质在生物精炼中的可持续性。可再生与可持续能源评论。

50, 925-941.

Norahim, N., Yaisanga, P., Faungnawakij, K., Charinpanitkul, T., Klaysom, C., 2018.

近期用于二氧化碳分离与捕获的膜技术进展。化学工程。

技术 41,211-223 。

Pal ，N. ，Agarwal ，M. ，2021. 材料加工与分离机制研究进展

膜向氢分离方向。《国际氢能期刊》46卷53页

27062-27087.

拉菲克，S. ，邓，L. ，哈格，M.-B. ，角色促进转运膜2016. of                                               和

用于高效捕获二氧化碳的复合膜——综述。ChemBioEng Rev. 3

(2), 68-85.

Rivero，J.R.，Nemetz，L.R.，Da    Conceicao，M.M.，Lipscomb，G.，Hornbostel，K.，

2023.平板膜模块中气体分离的建模： 流道尺寸变化的影响. 碳捕集科学与技术

6,100093.

Salleh，W.，Ismail，A.F.，2015. 用于气体分离过程的碳膜： 最新进展与未来展望. J.

Membr. Sci. Res. 1,2-15。

Sarangi ，P.K. ，Nanda ，S. ，2020. 通过暗发酵生产生物氢。

化学工程与技术 43 (4) ，601-612 。

Sazali ，N. ，2020. 关于使用聚合物膜分离H2/二氧化碳的简要综述。

J. 《先进流体力学与热科学》69卷174-182页。

Sazali ，N. ，Mohamed ，M. A. ，Salleh ，W.N.W. ，2020. 氢气分离用膜：一种

重要综述。国际先进制造技术杂志 107 (3-4) ，1859-1881 。

化工厂成本指数——化工

Tong，Z.，Ho，W.S.W.，2017. 用于二氧化碳分离与捕获的新型空间位阻聚乙烯胺膜J.

Membr. Sci. 543,202-211。

曾，H.-H. ，王，C.-T. ，章，G.-L. ，乌奇蒂尔，P. ，雷兹尼科娃，J. ，塞特尼科娃，K. ，

2016. 通过碳分子筛增强H2/甲烷和H2/二氧化碳的分离

二氧化钛修饰氧化铝载体上的膜：二氧化钛中间体的影响

层制备变量对界面粘附的影响。膜科学杂志 510,391-404 。

Turton ，R. ，Bailie ，R.C. ，Whiting ，W.B. ，Shaeiwitz ，J. A. ，2008. 分析、合成与

化学工艺设计。培生教育。

徐W. 、林德布拉森A. 、贾纳基拉姆S. 、安萨洛尼L. 、邓L. ，2023年。增强型二氧化碳/氢2

GO与PVA-GO嵌入PVAm纳米复合膜的分离效果

J. Membr. Sci. 671, 121397.

杨Y 、韩Y 、庞R 、何W.S.W. ，2020. 含胺膜

用于二氧化碳/氢气分离的功能化多壁碳纳米管膜

（巴塞尔）10,333 。

Younas ，M. ，Shafique ，S. ，Hafeez ，A. ，Javed ，F. ，Rehman ，F. ，2022. 《概述》

氢气生产：现状、潜力与挑战。Fuel 316, 123317 。

赵永新、何文森，2012年。立体位阻效应对固体胺类化合物的影响

用于二氧化碳传输的聚合物膜。《膜科学杂志》415卷，132-138页。

Zhao，Y.，Jung，B.T.，Ansaloni，L.，Ho，W.W.，2014. 多壁碳纳米管混合矩阵膜含胺用于高压二氧化碳/氢气分离。

J. Membr. Sci. 459, 233-243.